# copper mine operation and beneficiation, sulfide ore

Reference products = copper concentrate sulfide ore, molybdenite

## General comment

"For the mining and beneficiation of copper sulfide ores in Canada.

Background: Metals are produced as part of a complex, highly interconnected and interdependent system, with many desirable but scarce/critical metals recovered as by-products during the production of one or more ‘host’ metal(s). Copper is one of the world’s major mineral commodities and is mined from heterogeneous sulfide or oxide mineral deposits in countries worldwide. Copper sulfide deposits, such as those of the porphyry or massive sulphide type, contain numerous other valuable minerals, which are desirable to society. Copper is mined & beneficiated to produce a copper sulfide concentrate, as well as other by-product concentrates (e.g. molybdenite), which are sold to smelters. Copper sulfide concentrates are smelted to produce the intermediate product, copper anode. This is then sold to refineries, where it is electrorefined to produce copper cathode, which is sold to fabricators. The by-product of copper electrorefining is anode slime, which contains various important by-product metals (principally gold, silver, selenium & tellurium) and is sold to precious metal recovery plants for further processing to recover the valuable metals.

Modelling approach: This dataset was created using the life cycle inventory process model described by Classen et al. (2009) and used to generate datasets for ecoinvent v2.1. Typical average ore grades are estimated for each region based on data from Northey et al. (2014), while values for several other key input parameters have been updated since the release of the v2.1 dataset. These include (non-exclusively) the production volumes, beneficiation efficiency (i.e. yield), concentrate grades, anode slime composition (a product of the downstream copper electrorefining processing but that has a direct influence on the properties of exchanges in this dataset), and water outputs. Further information on these changes is provided in the Sampling Procedure comment, as well as the accompanying documentation (see Turner & Hischier, 2020).

References:

Classen, M., Althaus, H.-J., Blaser, S., Scharnhost, W., Tuchschmid, M., Jungbluth, N., & Emmenegger, M. F. (2009). Life cycle inventories of metals. Final report, ecoinvent data v2.1, No. 10. Dübendorf, Switzerland.

Northey, S., Mohr, S., Mudd, G. M., Weng, Z., & Giurco, D. (2014). Modelling future copper ore grade decline based on a detailed assessment of copper resources and mining. Resources Conservation and Recycling, 83, 190-201.

Turner, D. A. & Hischier, R. (2020). Life cycle inventories of pyrometallurgical copper production and anode slime processing. Empa, St. Gallen, Switzerland."

## Technology

Based on typical current technology. Mining is done 70% open pit and 30% underground, followed by joint beneficiation of copper and molybdenite trough flotation, where considerable amounts of agents are added. Overburden is disposed separate to sulfidic tailings near the mining site. No dewatering (or other pre-treatment) of the tailings of is assumed as this is considered a treatment activity that occurs only at selective sites and is therefore modelled separately.

## Included activities starts

Construction of mine site (including mill), including site excavation and facility installation.

## Included activities ends

Site closure; termination of mining and beneficiation activities and the deconstruction of the mine site.

## Synonyms

sulphide ore

## Product information

'copper concentrate, sulfide ore' is a metal. It has a 29.63% copper content, which is a transition metal. It is the direct product from mining and beneficiation and a by-product of smelting and refining of nickel concentrate. It is in a form of powder. It can be used in the following applications and/or processes: production of copper metal.

## Geography comment

This dataset is valid for the whole corresponding region. Some agents used, such as lime and sodium cynaide, originate from datasets value for Switzerland or Europe. Processes such as blasting originate from datasets value for Switzerland or Europe. Exchanges amounts calculated based on country-specific average ore grade (as reported in Northey et al. 2014).

References:

Northey, S., Mohr, S., Mudd, G. M., Weng, Z., & Giurco, D. (2014). Modelling future copper ore grade decline based on a detailed assessment of copper resources and mining. Resources Conservation and Recycling, 83, 190-201.

## Time period Comment

Production volumes are representative of the situation in 2015 but are considered valid until the end of 2019. Data sources for the inventory model have not been updated since v2.1 (see Classen et al. 2009), but important model parameters that determine input data to the model have been updated to be consistent with the current situation.

References

Classen, M., Althaus, H.-J., Blaser, S., Scharnhost, W., Tuchschmid, M., Jungbluth, N., & Emmenegger, M. F. (2009). Life cycle inventories of metals. Final report, ecoinvent data v2.1, No. 10. Dübendorf, Switzerland.

## Sampling procedure

All exchanges to the environment and from the technosphere calculated using the life cycle inventory model presented in Classen et al. (2009) for 'copper, molybdenum & telluride and silver containing byproducts' (ecoinvent v.2.1). All exchange values are calculated as a function of the mass of ore processed, which is itself a function of ore grade. To increase the temporal and geographical representativeness of the inventory, ore grades have been updated here (since v2.1) based on data from Northey et al. (2014). The estimated average copper ore grade in Canada is 0.31%. The amounts and composition (exchange properties) of 'copper concentrate, sulfide ore', 'molybdenute concentrate' and 'treatment of sulfidic tailings, from copper mine operation, tailings impoundment' were estimated based on a global material flow analysis of copper production. Key input data to the model include: production volumes of each metal, taken from the USGS Minerals Yearbook 2015; concentration yields (i.e. transfer coefficients for each element from Earth's crust to each product via mining and beneficiation), taken as the arithmetic mean of values reported in the literature; anode slime composition, from which the amounts of silver, gold, tellerium and selenium that are extracted from the Earth's crust during this activity are estimated, taken as the arithmetic mean of values reported in the literature; 'copper concentrate,sulfide ore' grade (26.7% Cu), taken from Delbeke & Rodriguez (2014); 'molybdenite concentrate' composition, taken as the arithmetic mean of values reported in the literature (48% Mo; 3.5% Cu). For more information, please refer to the accompanying documentation. References Classen, M., Althaus, H.-J., Blaser, S., Scharnhost, W., Tuchschmid, M., Jungbluth, N., & Emmenegger, M. F. (2009). Life cycle inventories of metals. Final report, ecoinvent data v2.1, No. 10. Dübendorf, Switzerland. Delbeke, K., & Rodriguez, P. H. (2014). Copper Concentrates - Environmental and Human Health hazard classification. Application to the assessment of substances “Harmful to the Marine Environment” (HME) as set out under the 2012 Annex V MARPOL Convention amendments. Santiago, Chile. Northey, S., Mohr, S., Mudd, G. M., Weng, Z., & Giurco, D. (2014). Modelling future copper ore grade decline based on a detailed assessment of copper resources and mining. Resources Conservation and Recycling, 83, 190-201.

# gold production

Reference product = gold

## General comment

This dataset describes the production of 1 kg of gold. Data was taken from the environmental report of Placer Dome Inc. for the Campbell, Musselwhite and Porcupine Mines, which produce only gold. Campbell and Musselwhite are underground mines, whereas Porcupine has underground and open pit mines. For the inventory, most by product and exchange amounts were calculated by adding the corresponding inputs or outputs of each mine, and then scaling them to the reference flow of 1 kg of gold. Since the mines have been sold in 2006 to Kinross Gold Corporation and Goldcorp Inc., no actual data is available. Both enterprises do not publish their environmental data. Therefore, data from 2002 is used to model the gold production in Canada.

[This dataset was already contained in the ecoinvent database version 2. It was not individually updated during the transfer to ecoinvent version 3. Life Cycle Impact Assessment results may still have changed, as they are affected by changes in the supply chain, i.e. in other datasets. This dataset was generated following the ecoinvent quality guidelines for version 2. It may have been subject to central changes described in the ecoinvent version 3 change report (http://www.ecoinvent.org/database/ecoinvent-version-3/reports-of-changes/), and the results of the central updates were reviewed extensively. The changes added e.g. consistent water flows and other information throughout the database. The documentation of this dataset can be found in the ecoinvent reports of version 2, which are still available via the ecoinvent website. The change report linked above covers all central changes that were made during the conversion process.]

Beneficiation, concentration and refinement of gold.

total requirements and emissions of the Campbell, Musselwhite and Porcupine Mines in 2002 as well as the total for Canada.

## Technology

OPEN PIT MINING:

The ore is mined in four steps: drilling, blasting, loading and hauling. In the case of a surface mine, a pattern of holes is drilled in the pit and filled with explosives. The explosives are detonated in order to break up the ground so large shovels or front-end loaders can load it into haul trucks.

UNDERGROUND MINING:

Some ore bodies are more economically mined underground. In this case, a tunnel called an adit or a shaft is dug into the earth. Sort tunnels leading from the adit or shaft, called stopes, are dug to access the ore. The surface containing the ore, called a face, is drilled and loaded with explosives. Following blasting, the broken ore is loaded onto electric trucks and taken to the surface. Once mining is completed in a particular stope, it is backfilled with a cement compound.

ORE AND WASTE HAULAGE:

The haul trucks transport the ore to various areas for processing. The grade and type of ore determine the processing method used. Higher-grade ores are taken to a mill. Lower grade ores are taken to leach pads. Some ores may be stockpiled for later processing.

BENEFICIATION:

In the Porcupine Mines, gold is recovered using a combination of gravity concentration, milling and cyanidation techniques. The milling process consists of primary crushing, secondary crushing, rod/ball mill grinding, gravity concentration, cyanide leaching, carbon-in-pulp gold recovery, stripping, electrowinning and refining.

In the Campbell Mine, the ore from the mine, after crushing and grinding, is processed by gravity separation, flotation, pressure oxidation, cyanidation and carbon-in-pulp process followed by electro-winning and gold refining to doré on site.

The Musselwhite Mine uses gravity separation, carbon in pulp, electro¬winning and gold refining to doré on site.

REFINING:

Wohlwill electrolysis. It is assumed that the gold doré-bars from both mines undergo the treatment of Wohlwill electrolysis. This process uses an electrolyte containing 2.5 mol/l of HCl and 2 mol/l of HAuCl4 acid. Electrolysis is carried out with agitation at 65 – 75 °C. The raw gold is intro-duced as cast anode plates. The cathodes, on which the pure gold is deposited, were for many years made of fine gold of 0.25 mm thickness. These have now largely been replaced by sheet titanium or tantalum cathodes, from which the thick layer of fine gold can be peeled off. In a typical electrolysis cell, gold anodes weighing 12 kg and having dimensions 280×230×12 mm (0.138 m2 surface) are used. Opposite to them are conductively connected cathode plates, arranged by two or three on a support rail. One cell normally contains five or six cathode units and four or five anodes. The maximum cell voltage [V] is 1.5 V and the maximum anodic current density [A] 1500 A/m2. The South African Rand refinery gives a specific gold production rate of 0.2 kg per hour Wohlwill electrolysis. Assuming a current efficiency of 95% the energy consumption is [V] x [A] / 0.2 [kg/h] = 1.63 kWh per kg gold refined. No emissions are assumed because of the purity and the high value of the material processed. The resulting sludge contains the PGM present in the electric scrap and is sold for further processing.

WATER EMISSIONS:

Effluents are discharged into the ocean.

REFERENCES:

Newmont (2004) How gold is mined. Newmont. Retrieved from http://www.newmont.com/en/gold/howmined/index.asp

Renner H., Schlamp G., Hollmann D., Lüschow H. M., Rothaut J., Knödler A., Hecht C., Schlott M., Drieselmann R., Peter C. and Schiele R. (2002) Gold, Gold Alloys, and Gold Compounds. In: Ullmann's Encyclopedia of Industrial Chemistry. Online version, posting date: September 15, 2000 Edition. Wiley-Interscience, Online-Version under: http://dx.doi.org/10.1002/14356007.a12_

Auerswald D. A. and Radcliffe P. H. (2005) Process technology development at Rand Refinery. In: Minerals Engineering, 18(8), pp. 748-753, Online-Version under: http://dx.doi.org/10.1016/j.mineng.2005.03.011.

## Included activities starts

From the transport of raw materials to the mine.

## Included activities ends

This activity ends with the Wohlwill electrolysis of gold. This data set includes the mining and beneficiation of the metals, the smelting, the energy, materials and land consumption, and the air and water emissions. This dataset does not include the emissions from the refining step.

## Product information

'gold' is a metal. It is soft and yellow, it is the most ductile and malleable of the metals. Refined gold has a purity of 99.50% and it is a transition metal. It is the direct product of mining, beneficiation and smelting gold ore, after being mined and beneficiated while it is the by-product of platinum group metals extraction and refinery operations. It can be used in the following applications and/or processes: coinage, ornaments, jewellery, gilding, textile industry, electronics, for high conductivity and suppressing secondary emissions, gold-plated grid wire, etc.

## Geography comment

Material requirements for gold concentration are estimated with Australian data, air emission are estimated with Swedish data.

# gold-silver mine operation and beneficiation

Reference products = copper concentrate sulfide ore, gold-silver ingot, lead concentrate, zinc concentrate

## Technology

The ore is mined in an underground mine and transported by trucks to the mill for further processing.

The ore is then fed into a series of grinding mills where steel balls grind the ore. Then follows the steps of flotation of copper and zinc, concentrate handling, cyanide destruction and backfilling of the tailings, refining of gold by electro-winning and melting in furnace to produce the gold and silver ingots. 20% of the tailings produce are sent underground to be used as backfill; sulfidic tailing is managed on site in tailings ponds.

## Included activities starts

From metal containing ore extraction from the ground.

## Included activities ends

This activity ends with the benefication of the concentrates and a first refining of the gold-silver ingots. The dataset includes underground mining, benefication, first refining of the ingots, waste rock piles, tailings ponds and wastewater treatment. This dataset doesn"t include : - Waste sent to recycling : Paper, cardboard, plastic, glass (3.129E0 kg/kg), batteries (1.865E-1 kg/kg), textiles (5.028E-2 kg/kg) - Waste sent back to provider for reuse : ink cartridges (1.658E-3 kg/kg) - Electro-winning : anode and cathode production and infrastructures. Also, emissions to air and water are limited to what has been measured on site.

## Product information

'gold-silver, ingot' is a metal. It is a mix of gold, silver and other impurities. They are both transition metals. It is the direct poduct of smelting gold and silver ore concentrate, after being mined and beneficiated. It is in a form of ingots. It can be used in the following applications and/or processes: jewelery manufacturing, metal alloys, in nanoparticles for biotechnology and biomedical field.

## Geography comment

Inputs and outputs relate to Quebec production.

## Time period Comment

The dataset represents the activity in 2012

## Sampling procedure

Specific data were collected on the only production site in Quebec.

## Extrapolations

Specific data were collected from the only mine in Quebec who produced all of these products from one ore. Extrapolation was done for the infrastructure based on dataset ""mine infrastructure, underground, non-ferrous metal"". Uncertainty has been adjusted accordingly.

# gold-silver mine operation with refinery

Reference products = gold, silver

## General comment

This dataset describes the production of gold and silver in Quebec (Canada) in 2012. This includes the operations at the mining site located in Quebec, i.e. mining, benefication and a first refining, which leads to the production of doré bars, containing gold, silver and impurities.

Specific data were collected from 3 mines that produced doré bars in Quebec. These mines represent about 98% of Quebec gold production and about 95% of Quebec silver production from combined gold-silver mines. Share is estimated as the production statistics for 2012-2013 are not published yet and considers gold-silver mines only (not gold and silver coming from other mines). One mine is an open-pit mine and the two others are underground. A weighted average of 839 tonnes of ore is extracted per kg of gold produce. The recovery rate of gold is known for two of the mines (89% and 91%) and the recovery rate of silver known for only one mine (76%).

Note that the mine infrastructure are extrapolated from gold-silver mine operation with refinery, GLO dataset, where the modelled mines are open pit. This is not representative of the Quebec situation where two of the three modelled mine are underground. Thus a mine infrastrucuture, gold and silver, Québec will eventually be created in order to reflect the Québec specificity.

In order to create a dataset with gold and silver as outputs (to comply with the boundaries of the GLO dataset), a very simplified modeling of the refining of the doré bars to produce gold and silver has been added to this dataset although it is done in Ontario (Canada) : electricity use is extrapolated from gold-silver mine operation with refinery, PE and PG datasets and infrastructure extrapolated from gold-silver mine operation with refinery, GLO dataset.

It is assume that the refining efficency is 100% (i.e. no loss of gold).

## Technology

One of the modelled mine is an open-pit mine and the two others are underground.

## Included activities starts

From metal containing ore extraction from the ground.

## Included activities ends

This activity ends with the refining of gold and silver. This dataset includes the operation at the mining site located in Quebec (Canada), i.e. mining, benefication and a first refining, which leads to the production of doré bars. The refining of the doré bars to produce gold and silver, occuring in Ontario (Canada) is also included in this dataset. Energy and material use, water and air emissions, infrastructure and land use are included for the operation at the mine site and only electricity and infrastructures are included for the refining of the doré bars. This dataset doesn"t include: - Fine charcoal (byproduct): fine charcoal coal that no longer meets specifications to enter the process is sent to a smelter to recover gold. Excluded because available data are not complete and reliable. - Waste sent to recycling: Paper, cardboard (1.028E1 kg/kg) and wood, metals, paper, oil (1.853E1 kg/kg). Note that the emissions to air and water are limited to what has been measured on site. Also, anodes and cathodes for doré bar refining are supposed to be included in refinery infrastructure. All calculations made can not be documented (using paramaters, properties and equation) for confidentiality reasons.

## Product information

'gold' is a metal. It is soft and yellow, it is the most ductile and malleable of the metals. Refined gold has a purity of 99.50% and it is a transition metal. It is the direct product of mining, beneficiation and smelting gold ore, after being mined and beneficiated while it is the by-product of platinum group metals extraction and refinery operations. It can be used in the following applications and/or processes: coinage, ornaments, jewellery, gilding, textile industry, electronics, for high conductivity and suppressing secondary emissions, gold-plated grid wire, etc.

## Geography comment

Inputs and outputs for mining, benefication and a first refining relate to Quebec production. Inputs for doré bar refining, which is done in Ontario, are extrapolated from dataset gold-silver mine operation with refinery (PG, CL, SE).

## Time period Comment

Collected data for Quebec industry for the years 2012 and 2013 : two mines provided 2012 data and one mine provided 2013 data (partly extrapolated as the year was not yet completed).

## Sampling procedure

Specific data were collected from 3 mines located in Quebec for mining, benefication and a first refining. Extrapolation based on ecoinvent datasets was done for the refining of the doré bars.

## Extrapolations

Extrapolations have been made for: - The refining of the doré bars based on ecoinvent datasets for electricity consumption and infrastructures. - Recovery rate of silver known for only one mine and supposed equivalent for all three mines. - Recovery rate of gold known for two mines and assumed equal to the average of the two mines for the third mine. - The chemicals used for wastewater treatment are known for the 2 smaller mines (different inputs) and extrapolated for the third mine. - Emissions to water: some emissions were given by one mine and extrapolated to the other 2 mines and other emissions were given by two mines and extrapolated to the third one. - Emissions to air extrapolated from 1 mine to the other two, based on gold production. - Waste were given by two mines and extrapolated to the third one. - Mine insfrastructure extrapolated from gold-silver mine operation with refinery, GLO dataset. The uncertainty has been adjusted accordingly.

# nickel mine operation and benefication to nickel concentrate, 16% Ni

## General comment

This dataset represents the production of 1 kg of nickel ore, beneficiated to 16% Ni in Quebec (Canada) for the year 2010.

This dataset is a disagreggation of the existing dataset ''nickel mine operation, sulfidic ore'', which contains smelting and refining on top of the mine operation. The disagreggation was done because primary data was available for nickel mine operation but not for subsequent stages of smelting and refining. Thus, the production volume of this dataset is already included in the global dataset ''nickel mine operation, sulfidic ore, GLO''. Until data on smelting and refining become available, this dataset cannot be used as part of a life cycle assessment.

The concentrate produced is composed of 16% Ni; 4% Cu; 0.24% Co; 0.61 g/t Au; 10.84 g/t Ag; 2.8 g/t Pt; 9.68 g/t Pd; 0.95 g/t Rh.

The sulfidic nickel ore is extracted in an underground mine, where 7.21 kg of ore are extracted per kg of concentrate produced. The recovery rate (metal in ore/metal in the concentrate) is 90% for Ni and 82% for Cu.

The concentrate produced is sent to a smelter located in Ontario (Canada) and to a refinery located in Norway (both excluded).

No specific data were available except for some emissions to water and air publicly available. Most of the data were taken from the Environmental Impact Assessment of the only Nickel mine in Quebec dated from 1993 and converted with a conversion factor (ore mined in 2010/expected amount of ore according to ElA). Some extrapolations were made based on ecoinvent datasets.

## Technology

Mining is done underground, followed by beneficiation. Overburden (2.67 kg/kg concentrate) and tailings (6.99 kg/kg concentrate) are disposed on the mining site.

## Included activities starts

Mining process starting from nickel ore, in ground.

## Included activities ends

This activity ends at the gate of the beneficiation plant. The dataset includes the extraction of nickel ore in an underground mine and it's benefication, management of tailings and waste rocks and wastewater treatment. The dataset does not include the end of life of the wasterwater sludge (no information available).

## Product information

'nickel concentrate, 16% Ni' is a metal. It has a 16% nickel content, which is a transition metal. It is the direct product from mining and beneficiation and by-product of cobalt production. It is in a form of powder. It can be used in the following applications and/or processes: production of nickel metal.

## Geography comment

This module represents the production of nickel concentrate in the Québec region.

## Time period Comment

The dataset represent the activity in 2010. Uncertainty has been adjusted accordingly.

## Sampling procedure

Estimations (Environmental Impact Assessment), specific data (National Pollutant Release Inventory (NPRI)) and extrapolation based on ecoinvent datasets.

## Extrapolations

Extrapolations were done for the following inputs: - ANFO (explosive and diesel): based on dataset ''iron mine operation and iron ore benefication to 65%, Québec 2011''. - Sand and cement: based on dataset ''nickel mine operation, sulfidic ore, GLO''. - Infrastructure (including landuse) : based on dataset ''nickel mine operation, sulfidic ore, GLO''