Supplementary Material

Life cycle impacts on climate change caused by metal production 
from deep-sea manganese nodules versus land-based deposits

Authors: Benjamin Fritza; Pia Heidaka; Jürgen Vastersb; Thomas Kuhnb; Gudrun Frankenb; Mario Schmidta*

a Institute for Industrial Ecology, Pforzheim University, Tiefenbronner Str. 65, 75175 Pforzheim, Germany
b Federal Institute for Geosciences and Natural Resources, Stilleweg 2, 30655 Hannover, Germany

*Corresponding authors:
Mario Schmidt, mario.schmidt@hs-pforzheim.de

Table of Contents

Abbreviations	3

I.	Detailed description of the metallurgical processing of manganese nodules	4

II.	Processes used for the LCA model of manganese nodule exploitation	5

III.	Procedure for comparing multi-product systems	6

IV.	Description of the mining projects representing the land-based product system	9

V.	Inventory Woodie Woodie	9

V.I.	Ferromanganese production (land-based)	9

V.II.	Mining	9

V.III.	Comminution	10

V.IV.	Transportation	12

V.V.	Metallurgy	13

VI.	Inventory Murrin Murrin	16

VI.I.	Nickel and cobalt production (terrestrial)	16

VI.II.	Extraction from nature	16

VI.III.	Comminution	17

VI.IV.	Metallurgy	17

VII.	Inventory Kevitsa	19

VII.I.	Production of copper, cobalt and nickel (terrestrial)	19

VII.II.	Extraction from nature	19

VII.III.	Comminution	20

VII.IV.	Transportation	22

VII.V.	Metallurgy	22

VIII.	Metal prices used in this study	24

IX.	Comparison of nodules and land-based climate impacts when applying alternative low emission electricity scenario	25

X.	Data quality assessment	25

References	28

## Abbreviations

ARD			Acid Rock Drainage
BGR			Federal Institute for Geosciences and Natural Resources Germany
e.g.			for example (Latin: exempli gratia)
FTP			Feed to plant
i.e.			this is (Latin: id est)

# Detailed description of the metallurgical processing of manganese nodules

Cathode copper, cathode nickel, cobalt powder and ferromanganese can be extracted from the nodules by applying a combination of reduction smelting steps and leaching in sulfuric acid. The nodules are ground and dried by direct contact with combustion gases of the coal burning to remove the water that is not chemically bound to the minerals (moisture content 40%). The manganese dioxide and iron (III) oxide are then reduced to manganese (II) and iron (II) oxides in the presence of coke with a carbon monoxide-rich generator gas at a high temperature (725°C). The hot roasted and pre-reduced product is then charged into an electric furnace together with coke and silica and smelted. In this step, most of the copper, nickel, cobalt and iron, as well as some manganese, are reduced (at 1425°C). A molten alloy phase is formed containing iron, copper, nickel and cobalt, among others, which separates by gravity from the unreduced but also molten manganese slag. The hot alloy is transferred to converter vessels where, with additional silica, the manganese and most of the iron are reoxidized with air, separated as slag and returned to the electric furnace. Gypsum and coke are then added to the alloy, resulting in a “matte” - i.e., a metal sulfide phase - containing copper, nickel and cobalt due to the sulfur produced by the reduction of the gypsum. Iron and manganese are bound as silicate in the converter slag. A second liquid-liquid separation is performed in the converter, where the slag is returned to the electric furnace and the “matte” is granulated by quenching in water. The electric furnace manganese slag together with recycled iron-rich slag from the conversion can be further reduced (at 1.480°C) with additional coke in an electric furnace to produce, if desired, a molten ferromanganese alloy that separates by gravity from the unreduced manganese slag. The ferromanganese is cast for sale, and the waste slag is granulated for disposal. The metals are recovered from the granulated matte by leaching in strong (5%), hot (110°C) sulfuric acid in the presence of oxygen (at 10 atm. pressure). The metal pregnant solution is subject to a series of purification steps in which it is contacted with an organic extractant. This selectively removes copper and nickel from the aqueous solution by means of ion exchange. Ammonia is added to the solution to control the pH during the extraction steps. The metals are recovered selectively from the organic liquid and transferred to acidic aqueous solutions in which copper and nickel sulfate accumulate.

From these solutions, cathode-copper and -nickel are produced by electrowinning. Cobalt is then recovered from the aqueous ammonium sulfate solution by contacting it with hydrogen sulfide. This way cobalt precipitates as insoluble sulfide as well as small amounts of copper, nickel and other metals that were not removed in the previous steps. The precipitate is removed from the aqueous ammonium sulfate solution and contacted with air and hot (100°C) sulfuric acid to selectively re-dissolve cobalt and the small amounts of nickel which are still present. The undissolved sulfides are sold as by-products, and cobalt and nickel are recovered from the solution in powder form by selective reduction with hydrogen at high pressure (34 atm. pressure) and high temperature (185 ° C). Lime is then added to the metal-free ammonium sulfate solution, and the mixture is contacted with steam (at 120 °C, 2 atm. pressure) to recover ammonia for reuse in the process. The gypsum formed in this step is combined with other solid and liquid process wastes and disposed of (Haynes et al., 1983).

Figure S 1: Simplified block flow diagram of the smelting and refining of manganese nodules following Haynes et al. (1983). The orange bars represent the processes used for the alternative allocation scenario.

# Processes used for the LCA model of manganese nodule exploitation

Table S 1: Names of the processes used from ecoinvent v.3.7.1 to model the LCA for manganese nodule according to the LCI found in figure 2 of the main manuscript

| Input (Collection of manganese nodules) |  |
| --- | --- |
| Flow according to figure 2 | Background process from ecoinvent v.3.7.1 |
| Energy from diesel for pumps | water pump operation, diesel (GLO, market for water pump operation, diesel) |
| Energy from diesel in marine engine | transport, freight, sea, bulk carrier for dry goods (GLO, market for transport, freight, sea, bulk carrier for dry goods) |
| Input (Transport of manganese nodules; distance: 1850 km) |  |
| Diesel engine vessel | transport, freight, sea, bulk carrier for dry goods (GLO, market for transport, freight, sea, bulk carrier for dry goods) |
| Input (pyro – hydrometallurgical refining of manganese nodules) |  |
| Water | tap water (PE, market for tap water) |
| Sulfuric acid | sulfuric acid (RoW, market for sulfuric acid) |
| Sodium Sulfate | sodium sulfate, anhydrite (RoW, market for sodium sulfate, anhydrite) |
| Sodium chloride | sodium chloride, powder (GLO, market for sodium chloride, powder) |
| Silica sand | silica sand (GLO, market for silica sand) |
| Quicklime | quicklime, milled, packed (RoW, market for quicklime, milled, packed) |
| Polyacrylamide | polyacrylamide (GLO, market for polyacrylamide) |
| Oxygen | oxygen, liquid (RoW, market for oxygen, liquid) |
| Nitrogen | nitrogen, liquid (RoW, market for nitrogen, liquid) |
| Lime | lime, packed (RoW, market for lime, packed) |
| Hydrogen | hydrogen, gaseous (GLO, market for hydrogen, gaseous) |
| Hydrogen sulfide | hydrogen sulfide (RoW, market for hydrogen sulfide) |
| Heavy fuel oil | heavy fuel oil (PE, market for heavy fuel oil) |
| Hard coal | hard coal (RLA, market for hard coal) |
| Gypsum | gypsum, mineral (RoW, market for gypsum, mineral) |
| Coke | coke (GLO, market for coke) |
| Chlorine | chlorine, gaseous (RoW, market for chlorine, gaseous) |
| Carbon black | carbon black (GLO, market for carbon black) |
| Boric acid | boric acid, anhydrous, powder (GLO, market for boric acid, anhydrous, powder) |
| Ammonia | ammonia, anhydrous, liquid (RLA, market for ammonia, anhydrous, liquid) |
| Graphite | graphite (GLO, market for graphite) |
| Electricity | electricity, medium voltage (MX, market for electricity, medium voltage) |
| Output (pyro – hydrometallurgical refining of manganese nodules) |  |
| Carbon dioxide | Carbon dioxide, fossil (emissions to air, non-urban air or from high stacks) |
| Inert waste | inert waste, for final disposal (RoW, market for inert waste, for final disposal) |
| Nickel smelter slag | nickel smelter slag (GLO, market for nickel smelter slag) |
| Waste gypsum | waste gypsum (RoW, market for waste gypsum) |

# Procedure for comparing multi-product systems

In our study, we used the product basket approach which accounts for the entire metal output from manganese nodules, while the environmental impacts of the land-based production need to be allocated and scaled to the equivalent product basket.

Figure A.1 schematically illustrates the applied procedure in this study. The deep-sea mine produces a bundle of metal co-products from manganese nodules with a fixed mass ratio. The compared product system which is compiled from various land mines also produces metal co-products, with a different metal composition and in a different ratio (a). To be able to make a comparison, the emissions of the land mines were distributed among their individual metals, i.e., an allocation must be performed according to monetary value (b).

In the further course, only those environmental impacts of the land mines are considered which are assigned to the metals that can also be extracted from manganese nodules (c). Based on this work, a fictitious terrestrial mine can then be assembled by scaling (d) and averaging (e) to produce the same metal composition as manganese nodule mining (f, h and i). In addition, an allocation to the individual metals can also be made for manganese nodule mining to compare their environmental impacts with the allocated environmental impacts of the land-based mine (g).

Figure S 2: Schematic description of the applied procedure for comparing multi-product systems

Continued on the next page

# Description of the mining projects representing the land-based product system

Kevitsa is characterized by a process route that includes physical pre-enrichment of the ore containing about 0.2 % Ni-eq to a concentrate at the mine site that is smelted and refined at the Ni smelter and refinery in Harjavalta, Finland (Boliden, 2021, Pittuck and Lepley, 2020). Murrin Murrin is a laterite leaching project with an average grade of approximately 1.1 % Ni-eq, which receives chemical inputs and electricity from natural gas on-site and from burning elemental sulfur (Dames & Moore, 1996a, EPA Australia, 1996, Minara Resources Pty Ltd, 2021). In terms of scope 1 and scope 2 emissions, both projects emit rather few greenhouse gases, meaning the two production chains belong to the low-emissive projects compared to the global Ni sector (Skarn Associates Limited, 2020). Using a sector-wide Ni industry average for assessing the CO2 intensity of land-based Ni production would potentially result in overestimating the Ni sector´s intensity since carbon-intensive ferronickel and nickel-pig iron production are included in the calculation of the average since both jointly account for 2/3 of global Ni production (Skarn Associates Limited, 2020). The other third of production with a low CO2 intensity relates to the class 1 nickel supply, which is comparable to the end product from manganese nodules´ processing as characterized by Dames & Moore and EIC Corporation (1977). The Woodie Woodie manganese project (Consolidated Minerals Limited, 2006a, Roberts and Francis, 2014) can be considered generic in terms of both extraction and further processing into FeMn, the latter step taking place in China where about 40 % of the global FeMn production is located. The average ore grade is about 40 % Mn which corresponds to approximately 0.8 % Ni-eq. Thus, the production route starting at Woodie Woodie can be assumed as moderately CO2-intensive for the manganese sector.

# Inventory Woodie Woodie

## Ferromanganese production (land-based)

The Woodie Woodie manganese mine in Western Australia serves as the basis for modeling terrestrial ferromanganese production. The manganese deposits have been known since the 1950s and have been mined in small-scale operations until commercial mining began in the 1990s. The mine processes about 3 Mt of ore per year into about 1.5 Mt of concentrate (Al Barazi et al., 2016). The concentrate is classified into a coarse (lumps) and a fine (fines) fraction.

Table A.1: Ore grade and stripping ratio of the land-based ferromanganese production model (Roberts and Francis, 2014).

| Ore grade FeMn [%] | Stripping ratio |
| --- | --- |
| 30 | 1:2 |

## Mining

Mining, e.g., excavation of pits and transport of ore and overburden, was modeled using the ecoinvent dataset of Classen et al. (2009) "manganese concentrate, at beneficiation - part mining". This source again is based on secondary literature from 1998 -2002, but the dataset can still be found in the most recent version of the ecoinvent v.3.8 database, with reference to a validity from January 1994 to December 2003. The dataset was scaled based on the amount of ore produced for further processing, i.e. process output. The stripping ratio in this source is 2.6:1, well above the value reported by Roberts and Francis (2014) for 2010 and 2011. The significantly higher stripping ratio is thus a conservative assumption that also fits well with the arithmetic mean stripping ratio reported by Barker (2020).

The following adjustments were made:

- the infrastructure share for underground was reduced from 30% to 0% and at the same time the surface share was increased from 70% to 100% since the Woodie Woodie mining project only produces above ground.

- According to Barker (2020), the risk of acid rock drainage (ARD) for Woodie Woodie is considered to be very low. All tailings are therefore modeled as non-sulfidic.

Table S 2 below shows the process data and the associated background processes used from ecoinvent v.3.7.1:

Table S 2: Process data and background data from ecoinvent of the land-based ferromanganese production model. Process step mining (Classen et al., 2009).

| Flow | Region | Dataset in LCA model | Amount | Unit |
| --- | --- | --- | --- | --- |
| Input (mining) |  |  |  |  |
| Mined rock (ore + overburden) | - | Material without upstream environmental impact | 7.69 | Mt |
| Energy from diesel combustion | Global | market for diesel, burned in diesel-electric generating set, 10MW | 141.04 | TJ |
| Explosives | Global | Market for blasting | 804.93 | t |
| Conveyor belts | Global | Market for conveyor belt | 231.51 | m |
| Mine infrastructure | Global | market for mine infrastructure, open cast, non-ferrous metal | 0.05 | unit |
| Output (mining) |  |  |  |  |
| Ore for processing | - | Intermediate product | 3.06 | Mt |
| Overburden | Global | market for non-sulfidic overburden, off-site | 4.65 | Mt |

## Comminution

The comminution (crushing and classification) process was modeled using data from publications specific to the Woodie Woodie Mine. The 2011 Consolidated Minerals LTD process chart found in Roberts and Francis (2014) provides a deeper understanding of the processes in the mine. The time period of the data used in this study is 2010-2011 according to Roberts and Francis (2014). The ore is first crushed and ground, and subsequently screened into four classes: direct lump and fines products, and for further crushing and classification into the fines and lumps routes, respectively. This results in the four sub-processes of crushing and classifying the ore, crushing and grinding the fines´ pre-product, crushing and grinding the lumps´ pre-product, and processing and transporting the resulting tailings to the tailings pond. Assumptions, such as those required to calculate mine energy requirements from machine metrics, are:

- The annual mine operating hours, such as those needed to calculate energy demand from machine performance data, were assumed to be 260 days. The value was given specifically for the Woodie Woodie Mine in Roberts and Francis (2014)

- A factor of 80% of full load was assumed as the payload compared to full load for the machine metrics (expert interview).

- The total water demand of the mine was divided equally among all processes of the crushing operation, as no other reference was available.

- The amount of tailings was split 35:7 between the associated routes based on the amount of fines´ and lumps´ products created (Roberts and Francis, 2014).

- Fines´ and lumps´ rejects from Roberts and Francis (2014) were conservatively modeled as non-sulfidic tailings.

- The total energy demand reported and its percentage allocation to type of consumer (e.g., compressors or office building) in Roberts and Francis (2014), which was not covered by the specific machine metrics, was divided equally among all processes in the comminution.

- The allocation of the different ore classes in this process was performed by mass, since the manganese contents are almost identical, according to Roberts and Francis (2014).

Table S 3 shows the process data and the associated processes used in ecoinvent v.3.7.1.

Table S 3: Process data and background data from ecoinvent of the land-based ferromanganese production model. Process step comminution (Roberts and Francis, 2014).

| Flow | Region | Dataset in LCA model | Amount | Unit |
| --- | --- | --- | --- | --- |
| Input (comminution) |  |  |  |  |
| Ore for processing | - | From upstream process „mining“ | 3.06 | Mt |
| Energy from diesel combustion | Global | market for diesel, burned in diesel-electric generating set, 10MW | 10.60 | TJ |
| Water | Global | market group for tap water | 7.50 | Mt |
| Output (comminution) |  |  |  |  |
| Ore for cyclone plant (fine fraction) | - | Intermediate product | 367.56 | kt |
| Tailings fraction for cyclone plant | - | Intermediate product | 161.83 | kt |
| Ore for drum plant (coarse fraction) | - | Intermediate product | 1.50 | Mt |
| Tailings fraction for drum plant | - | Intermediate product | 809.14 | kt |
| Coarse fraction for melting (lumps) | - | Intermediate product | 159.28 | kt |
| Fine fraction for sintering (fines) | - | Intermediate product | 67.39 | kt |
| Input (drum plant) |  |  |  |  |
| Ore for drum plant (coarse fraction) | - | From upstream process „comminution“ | 1.50 | Mt |
| Tailings fraction for drum plant | - | From upstream process „comminution“ | 809.14 | kt |
| Energy from diesel combustion | Global | market for diesel, burned in diesel-electric generating set, 10MW | 5.56 | TJ |
| Water | Global | market group for tap water | 7.50 | Mt |
| Ferrosilicon for density separation Suspended solids | Global | market for ferrosilicon | 596.70 | t |
| Output (drum plant) |  |  |  |  |
| Ore from drum plant (lumps) | - | Intermediate product | 1.08 | Mt |
| Tailings for tailings plant | - | Waste | 809.14 | kt |
| Tailings | Global | market for non-sulfidic tailing, off-site | 419.63 | kt |
| Input (cyclone) |  |  |  |  |
| Ore for cyclone plant (fine fraction) | - | From upstream process „comminution“ | 367.56 | kt |
| Tailings fraction for cyclone | - | From upstream process „comminution“ | 161.83 | kt |
| Energy from diesel combustion | Global | market for diesel, burned in diesel-electric generating set, 10MW | 3.51 | TJ |
| Ferrosilicon for density separation Suspended solids | Global | market for ferrosilicon | 176.43 | t |
| Water | Global | market group for tap water | 7.50 | Mt |
| Output (cyclone) |  |  |  |  |
| Ore from cyclone plant (fines) | - | Intermediate product | 202.16 | kt |
| Tailings for tailings plant | - | Waste | 161.83 | kt |
| Tailings | Global | market for non-sulfidic tailing, off-site | 162.34 | kt |
| Input (tailings plant) |  |  |  |  |
| Tailings from drum plant | - | Tailings (drum plant) | 809.14 | kt |
| Tailings from cyclone | - | Tailings (cyclone plant) | 161.83 | kt |
| Energy from diesel combustion | Global | market for diesel, burned in diesel-electric generating set, 10MW | 6.40 | TJ |
| Water | Global | market group for tap water | 7.50 | Mt |
| Organic chemicals | Global | market for chemical, organic | 24.27 | kt |
| Output (tailings plant) |  |  |  |  |
| Tailings | Global | treatment of non-sulfidic tailing, off-site | 970.97 | kt |

## Transportation

China is the largest ferromanganese producing country worldwide, comprising approximately 40 % of global market volume between 2007 and 2015 (IndexBox). Woodie Woodie exports the major part of mined ore (Consolidated Minerals Limited, 2006b) to China which had been confirmed by BGR (J. Vasters, personal communication, August 2022). The assumption is supported by the fact that since 2017, Woodie Woodie is privately owned by Ningxia Tianyuan Manganese Industry Co (TMI), a Chinese manganese producer who supplies approximately 19 % of overall Chines manganese ore imports (Consolidated Minerals Australia (ConsMin), 2020). Further, in Australia, only one refinery for ferromanganese exists and it is operated by a competitor which owns another manganese containing mine (Centre for Tasmanian Historical Studies, 2012).

Woodie Woodie is located close to Port Hedland which was assumed to be the exporting harbor. As refineries in China are widely dispersed (Metalshub, 2021) we browsed web portals such as made-in-china.com (Focus Technology) for regions covering lots of suppliers. Many refineries are located in the regions of Henan, Hebei and Tianjin. The harbor of Tianjin seems a reasonable import gate to these regions, so we assumed transport by ship to Tianjin port and an average truck distance to the center of the three mentioned Chinese regions.

For calculating the sea travel distance, we used the sea distance calculator from (ShipTraffic) which calculated the distance of 4386 nm (equivalent to 8122 km). For calculating truck distances, we used (Google) Maps. The distance from Port Hedland to Woodie Woodie amounts to 377 km. The average distance from Tianjin Port to the refinery was estimated at 380 km. Table S 4 shows the process data and the associated processes used in ecoinvent v.3.7.1.

Table S 4: Process data and background process from ecoinvent of the land-based ferromanganese production model. Process step transportation. Sources: (IndexBox); (Consolidated Minerals Limited, 2006b); (Metalshub, 2021); (Focus Technology); (ShipTraffic); (Google) Maps.

| Flow | Region | Dataset in LCA model | Amount | Unit |
| --- | --- | --- | --- | --- |
| Input (transportation) |  |  |  |  |
| Manganese ore, at mine (fines and lumps) | - | From upstream processes “cyclone”, “drum plant” and “comminution”. | 1.51 | Mt |
| Transport, by truck, from mine to Port of Hedland | Rest of World | market for transport, freight, lorry > 32 metric ton, EURO5 | 568.00 | Mt*km |
| Transport, by ship, from Port of Hedland to Port of Shanghai | Global | market for transport, freight, sea, bulk carrier for dry good. | 12240.00 | Mt*km |
| Transport, by truck, from Port of Shanghai to refinery | China | market for transport, freight, lorry > 32 metric ton, EURO5 | 573.00 | Mt*km |
| Output (transportation) |  |  |  |  |
| Manganese ore, at refinery (fines and lumps) | - | Intermediate product | 1.51 | Mt |

## Metallurgy

The Woodie Woodie mine produces lumps and fines as marketable products. However, since the comparative study of metal production from manganese nodules produces ferromanganese, additional processing steps must be appended after the production of lumps and fines. The metallurgical processing of lumps and fines to ferromanganese was modeled using the data sets from the study by the International Manganese Institute (2014). The fines are sintered prior to preparation in order to increase process stability in subsequent smelting. The data set was scaled with the respective quantities of lumps and fines. The reference year of the data set is 2010, according to the International Manganese Institute (2014). The following adjustments were made:

- The ratio of fines output to input in sintering was assumed to be 0.8, as stated by the International Manganese Institute (2014).

- The inputs "other Mn materials", "Si-materials", "Fe-materials" and "electrodes" in the melting process were not considered, according to the International Manganese Institute (2014).

- The International Manganese Institute (2014) does not specify emissions in the processes. Emissions for energy were covered by corresponding ecoinvent processes.

- The mass balance from metallic input and output was closed by waste processes.

Table S 5 below shows the process data and the associated processes used in ecoinvent v.3.7.1.

Table S 5: Process data and background data from ecoinvent for the land-based ferromanganese production model. Process step metallurgy (International Manganese Institute, 2014).

| Flow | Region | Dataset in LCA model | Amount |  | Unit |
| --- | --- | --- | --- | --- | --- |
| Input (sintering) |  |  |  |  |  |
| Fine fraction for sintering | - | From upstream process “transportation” | 67.39 |  | kt |
| Ore from cyclone plant | - | From upstream process “transportation” | 202.16 |  | kt |
| Electricity | China | market for electricity, medium voltage | 40.53 |  | TJ |
| Energy from coke combustion | Rest of World | Coke Industrial furnace | 390.00 |  | TJ |
| Lime | Rest of World | market for lime, packed | 6.88 |  | kt |
| Energy from coal combustion | Rest of World | Hard coal industrial furnace | 281.00 |  | TJ |
| Energy from heavy fuel oil combustion | Rest of World | heavy fuel oil, burned in refinery furnace | 32.26 |  | TJ |
| Output (sintering) |  |  |  |  |  |
| Fine fraction, sintered | - | Intermediate product | 205.76 |  | kt |
| Slag | Rest of World | Electric arc furnace slag | 63.79 |  | kt |
| Carbon dioxide emissions to air from lime neutralization | - | CO2, fossil [air/non-urban air or from high stacks] | 1.87 |  | kt |
| Input (smelting) |  |  |  |  |  |
| Ore (fines) | - | From upstream process “drum plant” |  | 1.08 | Mt |
| Coarse fraction for smelting (lumps) | - | From upstream process “comminution” |  | 159.28 | kt |
| Fine fraction, sintered (fines) | - | From upstream process “sintering” |  | 205.76 | kt |
| Electricity | Australia | market for electricity, medium voltage |  | 6.49 | PJ |
| Graphite | Global | market for graphite |  | 17.17 | kt |
| Water | Global | market group for tap water |  | 2.57 | Mt |
| Lime | Rest of World | market for lime, packed |  | 79.22 | kt |
| Energy from coal combustion | Rest of World | Hard coal industrial furnace |  | 2.21 | PJ |
| Energy from coke combustion | Rest of World | Coke Industrial furnace |  | 5.55 | PJ |
| Output (smelting) |  |  |  |  |  |
| Intermediate product after smelting | - | Intermediate product |  | 660.21 | kt |
| Slag | Rest of World | Electric arc furnace slag |  | 783.00 | kt |
| CO2 emissions (lime neutralization & electrodes) | - | CO2, fossil [air/non-urban air or from high stacks] |  | 85.20 | kt |
| Input (refining) |  |  |  |  |  |
| Intermediate product after smelting | - | From upstream process “smelting” | 660.21 |  | kt |
| Electricity | Australia | market for electricity, medium voltage | 430.04 |  | TJ |
| Energy from coke combustion | Rest of World | Coke Industrial furnace | 4.42 |  | TJ |
| Energy from natural gas combustion | Rest of World | Natural gas in industrial furnace | 74.99 |  | TJ |
| Water | Global | market group for tap water | 5.09 |  | Mt |
| Nitrogen | Rest of World | market for nitrogen, liquid | 12.11 |  | kt |
| Oxygen | Rest of World | market for oxygen, liquid | 78.74 |  | kt |
| Lime | Rest of World | market for lime, packed | 3.63 |  | kt |
| Output (refining) |  |  |  |  |  |
| Intermediate product after refining | - | Intermediate product | 605.69 |  | kt |
| Slag | Rest of World | Electric arc furnace slag | 54.52 |  | kt |
| CO2 emissions (lime neutralization) | - | CO2, fossil [air/non-urban air or from high stacks] | 1.02 |  | kt |
| Input (operation of the processing plant) |  |  |  |  |  |
| Intermediate product from refining | - | From upstream process “refining” | 605.69 |  | kt |
| Electricity | Australia | market for electricity, medium voltage | 1.02 |  | PJ |
| Energy from diesel combustion | Global | market for diesel, burned in diesel-electric generating set, 10MW | 130.00 |  | TJ |
| Flocculant | Global | polyacrylamide production | 6.06 |  | t |
| Chemicals | Global | Market chemicals inorganic | 72.00 |  | t |
| Energy from heavy oil combustion | Rest of World | heavy fuel oil, burned in refinery furnace | 80.84 |  | GJ |
| Energy from natural gas combustion | Rest of World | Natural gas in industrial furnace | 428.00 |  | TJ |
| Water | Global | market group for tap water | 60.57 |  | Kt |
| Lubricating oil | Rest of World | market for lubricating oil | 29.00 |  | t |
| Energy from gasoline combustion | Global | petrol, unleaded, burned in machinery | 6.90 |  | TJ |
| Energy from propane combustion | Rest of World | propane, burned in furnace | 4.38 |  | TJ |
| Energy from light fuel oil combustion | Rest of World | Light fuel oil in furnace | 130.00 |  | TJ |
| Output (operation of the processing plant) |  |  |  |  |  |
| Ferromanganese | - | Product | 605.69 |  | kt |

# Inventory Murrin Murrin

## Nickel and cobalt production (terrestrial)

The Murrin nickel-cobalt mine in Australia serves as the basis for modeling terrestrial nickel-cobalt production from lateritic ores. Extraction started in 1999. The mine is located in the Northeastern goldfields of Western Australia and produces approximately 35 kt of nickel and 3 kt of cobalt per year (Glencore plc, 2020). The mine produces energy from gas and steam turbines for use in its own operation. The same applies to sulfuric acid from sulfur and industrial gases from natural gas. Specifically, energy is generated from a 22 MW gas turbine and a 22 MW steam turbine, fueled by residual heat from the gas turbines and heat from the exothermic reaction of sulfuric acid production. The Murrin Murrin Mine requires large quantities of sulfuric acid and thus generates high volumes of acidic wastewater, which is neutralized with large quantities of limestone mined on site. Lime neutralization therefore accounts for a significant proportion of CO2 emissions at this mine.

Table S 6: Ore grade und stripping ratio of the nickel-cobalt production model (terrestrial) (Dames & Moore, 1996b, Wells, 2003).

| Ore grade |  | Stripping Ratio |
| --- | --- | --- |
| Co [g/t] | Ni [%] |  |
| 640 | 1 | 2:1 |

## Extraction from nature

Extraction from nature, e.g. the excavation of pits or mining and transport of ore and overburden, was modeled using the Nickel Institute dataset of Boonzaier (2020) "mining process for the production of ferronickel". The dataset was scaled based on the amount of the process output FTP (feed to plant). The data set is based on a stripping ratio of 3:1. The reference year of the data is 2017, according to Boonzaier (2020). We made the following adjustments:

- Energy demand from electricity and LPG was combined and modeled by gas turbines as described in Dames & Moore (1996b)

- According to Minara Resources Pty Ltd (2021), the risk of acid rock drainage for Woodie Woodie is considered to be very low. All tailings are therefore modeled as non-sulfidic.

Table S 7 shows the process data and the corresponding background processes from ecoinvent v.3.7.1.

Table S 7: Process data and corresponding background processes from ecoinvent for nickel-cobalt production. Process step extraction from nature (Boonzaier, 2020).

| Input (extraction from nature) |  |  |  |  |
| --- | --- | --- | --- | --- |
| Flow | Region | Dataset in LCA model | Amount | Unit |
| Mined rock (Ore + overburden) | - | Material without upstream environmental impacts | 17.53 | Mt |
| Energy from petrol combustion | Global | petrol, unleaded, burned in machinery | 1.81 | TJ |
| Explosives | Global | Market for blasting | 533.33 | t |
| Energy from diesel combustion | Global | diesel, burned in building machine | 1.14 | PJ |
| Lubricating oil | Rest of World | market for lubricating oil | 228.57 | t |
| Energy from natural gas production | Rest of World | Natural gas burned in turbine for compressor station | 50.29 | TJ |

| Output (extraction from nature) |  |  |  |  |
| --- | --- | --- | --- | --- |
| Ore for processing | - | Intermediate product | 4.00 | Mt |
| Waste | Global | municipal solid waste | 1.83 | t |
| Waste | Global | hazardous waste, for incineration | 1.20 | t |
| Overburden | Global | market for non-sulfidic overburden, off-site | 13.53 | Mt |
| Waste | Global | hazardous waste, for underground deposit | 380.95 | t |

## Comminution

Comminution was modeled specifically for the Murrin Murrin mine using data from (Dames & Moore, 1996b). The study was submitted to the Australian Environmental Protection Agency for peer review in 1995 and the mine opened in 1999. The reference year was in the future. Thus, similar to data basis of the deep-sea mining study, it is a technical feasibility study. The process diagram of Minara Resources Pty Ltd (2020) provide a deeper understanding of the mine. The ore is crushed and ground before entering the next process step metallurgy. Assumptions, such as those that were necessary to calculate the mines' energy requirements from machine metrics, are:

- The annual operating time of the mine which is e.g. needed for the calculation of energy demand from performance data of machines was assumed to be 330 days (J. Vasters, personal communication, November 2020).

- The efficiency of electricity generation from gas and steam turbine was assumed to be 50% (Kotowicz and Brzęczek, 2018).

- The energy use is divided between crushing and metallurgy in the ratio 20/80 (Boonzaier, 2020).

Table S 8 shows the process data and the corresponding background processes from ecoinvent v.3.7.1.

Table S 8: Process data and corresponding background processes from ecoinvent for nickel-cobalt production. Process step comminution (Dames & Moore, 1996b).

| Input (comminution) |  |  |  |  |
| --- | --- | --- | --- | --- |
| Flow | Region | Dataset in LCA model | Amount | Unit |
| Ore for processing | - | From upstream process | 4.00 | Mt |
| Water | Global | market group for tap water | 2.97 | Mt |
| Energy from natural gas combustion | Rest of World | Natural gas burned in turbine for compressor station | 320.30 | TJ |
| Output (comminution) |  |  |  |  |
| Crushed ore | - | Intermediate product | 3.80 | Mt |
| Overburden | Global | market for non-sulfidic overburden, off-site | 200.00 | kt |

## Metallurgy

The metallurgic processing of lateritic ore concentrates at Murrin Murrin was modeled using literature data from a technical feasibility study by Dames & Moore (1996). The models are based on the following assumptions:

- The annual operating time of the mine which is e.g. needed for the calculation of energy demand from performance data of machines was assumed to be 330 days (information provided by J. Vasters, personal communication, November 2020).

- The efficiency of electricity generation from gas and steam turbine was assumed to be 50% (Kotowicz and Brzęczek 2018).

- It is assumed that the mine uses only as much sulfur as it needs for leaching and does not use sulfur for additional power generation.

- The Murrin Murrin Mine generates electricity and industrial gases for use at the operation site from the two inputs of sulfur and natural gas. In Dames & Moore (1996), the total amount of natural gas and the required amount of industrial gases produced from it are given. From the amount of industrial gases (21 kt NH3, 14,000 Nm3/h H2, 33 kt H2S), the amount of natural gas required for generation was estimated using stoichiometry. An efficiency of 80% was assumed and included in the calculation. The amount of carbon contained in this amount of natural gas (CH4) was modeled entirely as CO2 emissions. We assumed that the difference between this amount of natural gas for industrial gas generation and the total amount of natural gas given in Dames & Moore (1996) is used for electricity generation.

- The energy use is divided between crushing and metallurgy in the ratio 20/80 (Boonzaier 2020).

- The "Emergency Venting Steam" mentioned in Dames & Moore (1996, Fig. 3.1) was not considered.

- Since Calcrete is not present in ecoinvent v.3.7.1, it is assumed to be limestone.

- Polyacrylamide is assumed to be the flocculant.

- Silicate sand is assumed to be the filter aid.

- The Ni-Co sulfide powder product was apportioned to the nickel and cobalt products, respectively, based on the metal contents (55% Ni, 5% Co, 40% residual).

- It was assumed that the difference between the amount of water withdrawn per year for the entire Murrin Murrin Mine and the process-specific data would be used in the refining.

Table S 9 shows the process data and the corresponding background processes from ecoinvent v.3.7.1.

Table S 9: Process data and corresponding background processes from ecoinvent for nickel-cobalt production. Process step metallurgy (Dames & Moore 1996)

| Input (metallurgy) |  |  |  |  |
| --- | --- | --- | --- | --- |
| Flow | Region | Dataset in LCA model | Amount | Unit |
| Crushed ore | - | From upstream process | 3.80 | Mt |
| Natural gas, for industrial gas production | Rest of World | Market for natural gas, high pressure | 6*E7 | Nm ³ |
| Energy from natural gas combustion | Rest of World | Natural gas burned in turbine for compressor station | 1282,6 | TJ |
| Sulfur | Global | market for sulfur | 490.00 | kt |
| Organic chemicals | Global | market for chemical, organic | 6.30 | t |
| Sodium carbonate for neutralization | Global | market for soda ash | 500.00 | t |
| Sodium hydroxide | Global | market for sodium hydroxide, without water, in 50 % solution state | 300.00 | t |
| Flocculant | Global | polyacrylamide production | 1.50 | kt |
| Acrylic acid | Rest of World | acrylic acid production | 221.00 | t |
| Filter additive | Global | market for silica sand | 45.00 | t |
| Oxygen from air separation | Rest of World | oxygen, liquid, (electricity deleted) | 50.00 | kt |
| Limestone | Rest of World | lime production, milled, packed | 900.00 | kt |
| Water | Rest of World | market for tap water | 4.55 | Mt |
| Output (metallurgy) |  |  |  |  |
| Ammonium sulfate | Product | AF: 2% | 70.00 | kt |
| Nickel | Product | AF: 82 | 43.00 | kt |
| Cobalt | Product | AF: 16 % | 3.10 | kt |
| NOx emissions to air | Global | Nitrogen oxides [air/unspecified] | 0.57 | kt |
| Carbon dioxide emissions to air | Global | Carbon dioxide, fossil [air/unspecified] (neutralization with lime + production of industrial gases) | 361.00 | kt |
| Sulfur dioxide emissions to air | Global | Sulfur dioxide [air/unspecified] | 6.67 | kt |
| Tailings (pH neutral) | Global | treatment of non-sulfidic tailing, off-site | 3.67 | Mt |

# Inventory Kevitsa

## Production of copper, cobalt and nickel (terrestrial)

The Kevitsa sulfide surface mine in North Finland, near the town of Sodankylä, is used as the basis for modeling terrestrial production of copper, nickel and cobalt. Concentrates from the Kevitsa mine are smelted into a nickel copper matte at Harjavalta, which is also refined at Harjavalta, at a different site. The mine's main products are copper and nickel concentrate, but also cobalt, platinum, palladium and gold. Exploration of the mine began in the late 1970s. Its annual production from about 7 Mt of ore is 28 kt copper, 21 kt nickel, 700 t cobalt, 1.5 t platinum, 1 t palladium and 600 kg gold (Boliden, 2020, Gray et al., 2016).

Table S 10: Ore grade and stripping ratio of the Kevitsa model (terrestrial) (Gray et al., 2016, Pittuck and Lepley, 2020).

| Ore grade |  |  |  |  |  | Stripping ratio |
| --- | --- | --- | --- | --- | --- | --- |
| Cu [%] | Co [%] | Ni [%] | Au [g/t] | Pd [g/t] | Pt [g/t] |  |
| 0.34 | 0.01 | 0.24 | 0.07 | 0.12 | 0.17 | 4.5:1 |

## Extraction from nature

Extraction from nature, e.g. the excavation of pits or mining and transport of ore and overburden, was originally modeled using the Nickel Institute dataset of Boonzaier (2020) "mining process for the production of nickel sulphate". During the review process, it was pointed out that the stripping ratio of 1:3 given in Boonzaier (2020) did not fit the Kevitsa mine. Data from the Skarn Associates Limited (2020) mining database specific to the Kevitsa Mine was therefore used. The reference year of the data from Skarn Associates Limited (2020) is 2018, and only data on electricity consumption can be found in the database. Additionally, the amount of explosives was added with 1 g/kg ore (Classen et al. 2009; Boonzaier 2020). The tailings were modeled using ecoinvent data sets on sulfidic tailings and thus include common assumptions for emissions as well as the risk for acid rock drainage (ARD). ARD is relevant at this mine because it is a sulfidic deposit.

Table S 11 shows the process data and the corresponding background processes from ecoinvent v.3.7.1.

Table S 11: Process data and corresponding background processes from ecoinvent for copper-nickel-cobalt production (terrestrial). Process step extraction from nature (Boonzaier, 2020, Skarn Associates Limited, 2020)

| Input (extraction from nature) |  |  |  |  |
| --- | --- | --- | --- | --- |
| Flow | Region | Dataset in LCA model | Amount | Unit |
| Mined rock (ore + overburden) | - | Material without upstream environmental impacts | 49.00 | Mt |
| Explosives | Europa | Blasting | 8.90 | kt |
| Energy from diesel combustion | Global | diesel, burned in building machine | 1.36 | PJ |
| Output (extraction from nature) |  |  |  |  |
| Ore for processing | - | Product | 8.91 | Mt |
| Tailings, sulfidic | Global | market for sulfidic tailings, from copper mine operation | 40.00 | Mt |

## Comminution

The comminution process which includes crushing and classification was modeled specifically for the Kevitsa Mine using data from publications. According to the process diagram from Gray et al. (2016), the ore is crushed first and classified into screens. The coarse fraction passes first through the autogenous mill (AG Mill) and then through the pebble mill (Metso Outotec HIGmill™). The finer fraction goes directly to the Pebble Mill. Finally, a stock stream of ground and digested ore goes to flotation, which is why we consider these processes as a closed black box. Subsequently, the first thing to be separated during copper flotation is the copper concentrate. The remainder moves on to the nickel flotation process step. Here, the nickel concentrate (with about 20% copper content) and a residue are produced, which are processed in the last flotation for the tailings tank. The reference year is 2014 – 2016 (Gray et al. 2016). Assumptions, such as those that were necessary for calculating the energy demand of the mines from machine key figures, are:

- The annual operating time of the mine, which is e.g. needed for the calculation of energy demand from performance data of machines, was assumed to be 330 days (J. Vasters, personal communication, November 2020).

- The operational load of the machines was assumed to be 80% of the full load.

- Since operational data for the HIG Mill could not be found in Gray et al. (2016), specific data for the Kevitsa Mine HIG Mill at 700 kW were taken from Lehto et al. (2016).

- The total water demand of the mine was divided equally between all processes of crushing and flotation.

- The FTP, i.e. the input to the comminution is equal to the output, resulting in no losses.

- According to Gray et al. (2016), the mine crushes about 40% in stockpiles to compensate for price fluctuations. This portion was not considered for this study. The data only refer to the amount of ore that later enters metal production.

- The frothing agent Nasfroth was assumed to be a non-specific organic chemical.

- For the flotation agent, sodium dithiophosphinate was assumed to be a typical inorganic chemical. For organic chemicals, we used sodium ethyl xanthate and potassium amyl xanthate as proxies. The corresponding data sets were taken from ecoinvent v.3.7.1.

- The amount of CO2 emissions to air during neutralization of leaches with limestone was determined analogous to the Murrin Murrin mine, resulting in 0.28 kg CO2/kg limestone.

- The total power consumption for supplying compressed air for the flotation was proportionally divided among copper, nickel and tailings flotation. We used the same proportions as the reported specific values of the flotation cells from the three flotations.

Table S 12 shows the process data and the corresponding background processes from ecoinvent v.3.7.1.

Table S 12: Process data and corresponding background processes from ecoinvent for copper-nickel-cobalt production (terrestrial). Process step comminution (Gray et al., 2016).

| Input (comminution) |  |  |  |  |
| --- | --- | --- | --- | --- |
| Flow | Region | Dataset in LCA model | Amount | Unit |
| Ore for processing | - | From upstream process | 8.91 | Mt |
| Electricity | Finland | market for electricity, medium voltage | 676.80 | TJ |
| Water | Switzerland | market for tap water | 412.50 | kt |
| Output (comminution) |  |  |  |  |
| Crushed ore | - | Intermediate product | 8.91 | Mt |
| Input (Cu-Flotation) |  |  |  |  |
| Crushed ore | - | From upstream process | 8.91 | Mt |
| Limestone | Europe | lime production, milled, packed | 677.16 | t |
| Organic chemicals | Global | market for chemical, organic | 418.77 | t |
| Inorganic chemicals | Global | market for chemical, inorganic | 106.92 | t |
| Electricity | Finland | market for electricity, medium voltage | 57.24 | TJ |
| Water | Switzerland | market for tap water | 137.50 | kt |
| Output (Cu-Flotation) |  |  |  |  |
| Flotation product, Ni-containing | - | Intermediary product | 8.84 | Mt |
| Copper concentrate | - | Intermediary product | 67.39 | kt |
| Carbon dioxide (Lime neutralization) | Global | Carbon dioxide, fossil [air/unspecified] | 189.60 | t |
| Input (Ni-Flotation) |  |  |  |  |
| Flotation product, Ni-containing | - | From upstream process | 8.84 | Mt |
| Organic chemicals | Global | market for chemical, organic | 923.97 | t |
| Water | Switzerland | market for tap water | 137.50 | kt |
| Electricity | Finland | market for electricity, medium voltage | 142.20 | TJ |
| Output (Ni-flotation) |  |  |  |  |
| Nickel concentrate | - | Intermediary product | 95.04 | kt |
| Tailings, to tailings plant | - | Waste | 8.74 | Mt |
| Input (Tailings flotation) |  |  |  |  |
| Tailings aus Flotation | - | From upstream process | 8.74 | Mt |
| Electricity | Finland | market for electricity, medium voltage | 21.24 | TJ |
| Organic chemicals | Global | market for chemical, organic | 356.40 | t |
| Water | Switzerland | market for tap water | 13.50 | kt |
| Output (Tailings flotation) |  |  |  |  |
| Tailings, sulfidic | Global | market for sulfidic tailings, from copper mine operation | 8.74 | Mt |

## Transportation

As the metallurgical processing of ore takes place in Harjavalta, Finland, transportation from the Kevitsa mine to the site is needed. We assumed rail transport for passing the distance of 924 km which we calculated by using the rail distance calculator provided by the European Commission (2022). Table S 13 shows the process data and the corresponding background processes from ecoinvent v.3.7.1.

Table S 13: Process data and corresponding background processes from ecoinvent for copper-nickel-cobalt production (terrestrial). Process step transportation (European Commission (2022)).

| Flow | Region | Dataset in LCA model | Amount | Unit |
| --- | --- | --- | --- | --- |
| Input (Transportation) |  |  |  |  |
| Copper concentrate | - | From upstream process | 67.39 | kt |
| Nickel concentrate | - | From upstream process | 95.04 | kt |
| Transport, by rail, from Kevitsa mine to Harjavalta plant | Finland |  | 150.00 | Mt*km |
| Output (Transportation) |  |  |  |  |
| Copper concentrate, at refinery | - | Intermediary product | 67.39 | kt |
| Nickel concentrate, at refinery | - | Intermediary product | 95.04 | kt |

## Metallurgy

The metallurgy and the processing of nickel-copper concentrates from the Kevitsa mine at the Harjavalta smelter are taken from the environmental study of the Finnish Environmental Institute Riekkola-Vanhanen (1999) and apply specifically to the Harjavalta copper smelter. The Harjavalta smelter also still processes ores from other mines. However, in the Riekkola-Vanhanen (1999) study, all values are always given scaled to one kilogram of copper or nickel output. The values were scaled using the quantities of concentrate reported in Gray et al. (2016). In addition, the amounts of cobalt and PGMs were not reported in Gray et al. (2016). These were scaled from Boliden (2020) using the ore volumes from Gray et al. (2016). The reference years are 1997 and 1998 according to Riekkola-Vanhanen (1999, p. 22ff.).

We made the following assumptions:

- "Oil & solvents (hazardous)," "filter materials (hazardous)," and "batteries and lamps (hazardous)" were combined as "hazardous waste for incineration".

- To balance the mass inputs and outputs of the process, we modeled nickel smelter slag as an additional output. For the treatment, we applied the treatment for nickel smelter slag from ecoinvent 3.7.1.

- Analogous to the preparation of manganese nodules and according to Dames & Moore and EIC Corporation (1977), the amount of silica sand used in metallurgy was assumed to be 18 kg sand/ kg Ni.

- According to critical review (expert in metallurgy), the amount of electrode material was assumed to be 2-3 kg/ t feed (resulting in 3.7 times the amount of CO2 from electrode burnup)

- In the source which we used for modelling the processing (Riekkola Vanhanen, 1999), only a precursor of nickel is produced. According to the BGR, the further processing of the precursor is considered to be similar to the processing of manganese nodules according to Dames & Moore (1977) (see Table 5). Therefore, the following specific chemical consumptions are scaled to the final nickel product (10.45 kt): 2.4 kg H2SO4, 1.89 kg lime (process-specific 0.28 kg CO2/kg lime), 2.5 kg quicklime, 0.11 kg H2S and 0.06 kg NH3.

Table S 14 shows the process data and the corresponding background processes from ecoinvent v.3.7.1.

Table S 14: Process data and corresponding background processes from ecoinvent for copper-nickel-cobalt production (terrestrial). Process step metallurgy (Riekkola-Vanhanen, 1999).

| Input (Metallurgy) |  |  |  |  |
| --- | --- | --- | --- | --- |
| Flow | Region | Dataset in LCA model | Amount | Unit |
| Nickel concentrate | - | From upstream process | 95.04 | kt |
| Copper concentrate | - | From upstream process | 67.39 | kt |
| Energy from heavy fuel oil combustion | Europe | heavy fuel oil, burned in refinery furnace | 299.16 | TJ |
| Electricity | Finland | market for electricity, medium voltage | 429 | TJ |
| Silicate sand | Global | market for silica sand | 188 | t |
| Graphite | Global | market for graphite | 406 | t |
| Sulfuric acid | Global | Market for sulfuric acid | 25 | t |
| Lime | Rest of World | lime production, milled, packed | 19 | t |
| Quicklime | Rest of World | quicklime production, milled, packed | 26 | t |
| Hydrogen sulfide | Rest of World | market for hydrogen sulfide | 1.1 | t |
| Ammonia | Rest of World | market for ammonia, liquid | 627 | kg |
| Output (Metallurgy) |  |  |  |  |
| Palladium | Product | AF: 7 % | 1.10 | t |
| Gold | Product | AF: 7 % | 646.85 | kg |
| Platinum | Product | AF: 15 % | 1.48 | t |
| Cobalt | Product | AF: 6 % | 635.02 | t |
| Nickel | Product | AF: 34 % | 10.45 | kt |
| Copper | Product | AF: 31 % | 19.22 | kt |
| Slags, to landfill | Switzerland | Waste gypsum landfill | 0.85 | kt |
| Waste | Switzerland | market for hazardous waste, for incineration | 95.8 | t |
| Slags, for treatment | Switzerland | treatment of nickel smelter slag, residual material landfill | 132 | kt |
| Carbon dioxide (lime neutralization) |  | Carbon dioxide, fossil [air/non-urban air or from high stacks] | 5.32 | t |
| Carbon dioxide from electrode burn-off |  | Carbon dioxide, fossil [air/non-urban air or from high stacks] | 1.49 | kt |

# Metal prices used in this study

Table S 15 shows the prices used for the metals in this study. The prices are average values from at least 5 years, rounded to two significant digits. Nuss and Eckelman (2014) show in their study that the allocation factors for all metals in ecoinvent, except for some rare earth metals, remain stable with changes in the time series (from five to 15 years). Therefore, we consider our assumption as sufficiently robust against price changes.

Table S 15: Metal prices (five-year averages) used in this study

| Product | Price[€/kg] | Comment |
| --- | --- | --- |
| Ferromanganese | 0.78 | Average 2010-16 based on BGR (2019) |
| Cobalt | 28 | Average 2013-17 based on USGS (2022) |
| Nickel | 10 | Average 2013-17 based on USGS (2022) |
| Copper | 5 | Average 2013-17 based on USGS (2022) |
| Palladium | 19900 | Average 2013-17 based on USGS (2022) |
| Platinum | 31200 | Average 2013-17 based on USGS (2022) |
| Gold | 34100 | Average 2013-17 based on USGS (2022) |
| Ammonium sulfate crystals | 0.16 +- 0.05 | Mean values from different trading platforms in Turkey, Vietnam, Europe, USA, World and China (e.g. Chou et al. (2005), Alibaba.com, Indiamart.com) |
| Ni-Co-sulfite powder | 7.2 | Calculated from 60 % Ni-Co content; this share was again divided between Ni and Co based on ore content, based on data from Dames & Moore (1996) |
| Zn-Cu powder | 3 | Assumption: price must be higher than zinc but lower than copper. |

# Comparison of nodules and land-based climate impacts when applying alternative low emission electricity scenario

Figure S 3: Influence of the alternative low-emissions energy scenario on the impact on climate change for land-based and deep sea metals in the product basket.

# Data quality assessment

Data quality was analyzed for the most relevant processes of the foreground systems of the land-based models, based on the ecoinvent pedigree matrix according to Ciroth et al. (2016). This means that for those processes whose inputs and outputs contribute more than 5 % to the overall GWP, an explicit data quality assessment takes place. Quality is assessed by five indicators: reliability and completeness of data, and temporal, geographic and technological correlation. The scale used for the measurement is numerical with the values 1, 2, 3, 4 and 5, where 1 represents the best quality and 5 the worst quality.

The modeling of deep-sea mining follows a prospective approach by using feasibility studies as data basis for the material flow model. In this context, the Pedigree matrix is not useful for an evaluation of the data quality, since the characteristics focus on existing production processes. It can be assumed that the described processes represent the current best practice case from a technological point of view. However, uncertainties remain with regard to the geographical and temporal correlation, since no concrete production capacities have yet been established.

Table S 16: ecoinvent pedigree matrix according to Ciroth et al. (2016)

|  | Reliability | Completeness | Temporal correlation | Geographic correlation | Technological correlation |
| --- | --- | --- | --- | --- | --- |
| 1 | Verified data based on measurements | Representative data from all sites relevant for the market considered, over an adequate period to even out normal fluctuations | Less than 3 years of difference to the time period of the data set | Data from area under study | Data from enterprises, processes and materials understudy |
| 2 | Verified data partly based on assumptions or non-verified data based on measurements | Representative data from > 50% of the sites relevant for the market considered, over an adequate period to even out normal fluctuations | Less than 6 years of difference to the time period of the data set | Average data from larger area in which the area under study is included | Data from processes and materials under study (i.e. identical technology) but from different enterprises |
| 3 | Non-verified data partly based on qualified estimates | Representative data from only some sites (<< 50%) relevant for the market considered or > 50% of sites but from shorter periods | Less than 10 years of difference to the time period of the data set | Data from area with similar production conditions | Data from processes and materials under study but from different technology |
| 4 | Qualified estimate (e.g. by industrial expert) | Representative data from only one site relevant for the market considered or some sites but from shorter periods | Less than 15 years of difference to the time period of the data set | Data from area with slightly similar production conditions | Data on related processes or materials |
| 5 | Non-qualified estimates | Representativeness unknown or data from a small number of sites and from shorter periods | Age of data unknown or more than 15 years of difference to the time period of the data set | Data from unknown or distinctly different area (North America instead of Middle East, OECD-Europe instead of Russia) | Data on related processes on laboratory scale or from different technology |

The following tables represent the data quality assessments of all three land-based projects.

Table S 17: Pedigree matrix for assessing the data quality of the Woodie Woodie model

Table S 18: Pedigree matrix for assessing the data quality of the Murrin Murrin model

Table S 19: Pedigree matrix for assessing the data quality of the Kevitsa model

The analysis of the data quality entries shows that the data entries for all mines can be considered complete, correspond to the geographic conditions and cover the technologies used in the mines well or very well. Only the modeling of the metallurgical processes in Kevitsa had to be supplemented by data of comparable processes in agreement with independent experts who enacted as critical reviewers of our study.

The temporal correlation is moderate, especially for Murrin Murrin, but also for the metallurgical processes of the Kevitsa model. This results from the older sources used to model these processes. But since the currently used technologies are well covered by these data and no significant changes in inputs and outputs have occurred in the meantime, the temporal correlation plays a rather minor role and should not have a significant impact on the representativeness of the data.

When considering the reliability of the data, there are significant differences between the models. The model for Woodie Woodie performs comparatively well and is based on verified data, some of which are based on assumptions, or on unverified data, but based on measurements. In contrast, Murrin Murrin's modeling for crushing electricity demand and for various metallurgy inputs uses only expert estimates or even so-called "unqualified" estimates. This results from the fact that the Murrin Murrin Mine produces its own required electricity and industrial gases on site from the two inputs of sulfur and natural gas. In the source used for the mine (Dames & Moore, 1996) the total amount of natural gas and the required amount of industrial gases produced from it are given. The allocation of the total quantity to the individual processes was made using the assumptions described in supplementary material section III.

For the Kevitsa modeling, again, non-verified data was used for the metallurgical processes, some of which were based on expert estimates. However, the ore mining and crushing assessments are of good quality. Inadequacies of the data in terms of their reliability for Kevitsa and Murrin Murrin, as well as for Kevitsa in terms of technological correlation in metallurgy, could possibly influence the assessment of the metals nickel, copper and cobalt. However, comparisons with literature values in have shown that the CO2-eq. per kg of metal for all mines are essentially within the range of literature values.

The predominantly good data quality of the Woodie Woodie model indicates that the results for terrestrial ferromanganese from this mine can be considered reliable despite the high specific GWP results per kg of FeMn.

References

Al Barazi S, Elsner H, Kärner K, Liedtke M, Schmidt M, Schmitz M et al. Mineralische Rohstoffe in Australien - Investitions- und Lieferpotenziale. 2015th ed. Berlin: DERA; 2016.

Barker J. Woodie Continued Operations Project: EPA Referral Supporting Document. West Perth, Australia: ConsMin; 2020.

BGR. Deutschland – Rohstoffsituation 2018. Hannover: Bundesanstalt für Geowissenschaften und Rohstoffe; 2019.

Boliden. Annual and Sustainability Report 2019. Stockholm, Sweden: Boliden AB, Stockholm; 2020.

Boliden. Annual and Sustainability Report. Stockholm, Sweden; 2021.

Boonzaier S. Life Cycle Assessment of Nickel Products. Ontario, Canada: The Nickel Institute; 2020.

Centre for Tasmanian Historical Studies. TEMCO; 2012, https://www.utas.edu.au/library/companion_to_tasmanian_history/T/TEMCO.htm [retrieved November 2022].

Ciroth A, Muller S, Weidema B, Lesage P. Empirically based uncertainty factors for the pedigree matrix in ecoinvent. Int J LCA 2016;21(9):1338–48.

Classen M, Althaus H-J, Tuchschmid M, Jungbluth N. Life Cycle Inventories of Metals Data v2.1: Part IX - Gold and Silver. Dübendorf: ecoinvent; 2009.

Consolidated Minerals Australia (ConsMin). Our story; 2020, https://www.consminerals.com.au/our-story [retrieved 07.11.22].

Consolidated Minerals Limited. Quarterly Activities Report for the quarter ended 31 December 2005: Highlights; 2006a.

Consolidated Minerals Limited. Quarterly activities report for the quarter ended 31 December 2005: Highlights; 2006b.

Dames & Moore. Murrin Murrin Nickel-Cobalt Project: Consultative Environmental Review. South Perth, Australia: Anaconda Nickel NL; 1996a.

Dames & Moore. Murrin Murrin Nickel-Cobalt Project: Consultative Environmental Review. South Perth, Australia: Anaconda Nickel NL; 1996b.

Dames & Moore, EIC Corporation. Description of Manganese Nodule Processing Activities for Environmental Studies. Processing Systems Technical Analysis 1977(Vol. III.):540 pp.

EPA Australia. Nickel/Cobalt ore mining and processing operations, Murrin Murrin, 60km east of Leonora: Anaconda Nickel NL. Report and recommendations of the Environmental Protection Authority. Perth, Australia: Anaconda Nickel NL; 1996.

European Commission. Calculate unit costs for eligible travel costs: Rail calculator; 2022, https://ec.europa.eu/info/funding-tenders/procedures-guidelines-tenders/information-contractors-and-beneficiaries/calculate-unit-costs-eligible-travel-costs_en [retrieved 28.07.22].

Focus Technology. Supplier discovery: Ferro manganese.

Glencore plc. Annual Report 2019. Baar, Switzerland: Glencore.com; 2020.

Google. Google Maps, https://www.google.de/maps [retrieved 28.07.22].

Gray D, Cameron T, Briggs A. Kevitsa Nickel Copper Mine, Lapland, Finland: NI 43-101 Technical Report. West Perth, Australia: First Quantum Minerals Ltd; 2016.

Haynes BW, Law SL, Maeda R. Updated Process Flowsheets for Manganese Nodule Processing: U.S. Department of the Interior, Bureau of Mines; 1983.

IndexBox. Global Ferro Manganese Production. Market Data Platform, https://www.indexbox.io/ [retrieved 28.07.22].

International Manganese Institute. Lifecycle Assessment of Global Manganese Alloy Production. Paris, France: International Manganese Institute; 2014.

Kotowicz J, Brzęczek M. Analysis of increasing efficiency of modern combined cycle power plant: A case study. Energy 2018;153:90–9.

Lehto H, Musuku B, Keikkala V, Kurki P, Paz A. Developments in Stirred Media Milling Testwork and Industrial Scale Perfomance of Outotec HIGMill; 2016, https://www.stmminerals.com/files/1557998239_Developments_in_stirred_media_milling_testwork_and_industrial_scale.pdf.

Metalshub. The top 20 Ferromanganese (HCFeMn) producers in the world; 2021, https://www.metals-hub.com/blog/top-high-carbon-ferromanganese-hcfemn-producers-in-the-world/ [retrieved 28.07.22].

Minara Resources Pty Ltd. Producing nickel and cobalt at Murrin Murrin; 2020, https://www.minara.com.au/who-we-are/producing-nickel-and-cobalt-at-murrin-murrin [retrieved Nov. 2020].

Minara Resources Pty Ltd. Murrin Murrin Nickel Cobalt Project - 17 Series Inpit Tailings Storage Facility Mining Proposal and Works Approval Application. Perth, Australia: Murrin Murrin Operations Pty Ltd; 2021.

Nuss P, Eckelman MJ. Life cycle assessment of metals: a scientific synthesis. PloS one 2014;9(7):e101298.

Pittuck M, Lepley B. Technical Report for the Kevitsa Cu-Ni-PGE Mine, Finland. Petikula, Finland: SRK Consulting; 2020.

Riekkola-Vanhanen M. Finnish expert report on best available techniques in nickel production. Helsinki, Finnland: Finnish Environment Institute; 1999.

Roberts DJ, Francis RS. Woodie Woodie Operations, Consolidated Minerals Pty Ltd. Australasian Mining and Metallurgical Operating Practices 2014:1863–78.

ShipTraffic. Sea route & distance, http://www.shiptraffic.net/2001/05/sea-distances-calculator.html [retrieved 28.07.22].

Skarn Associates Limited. GHG & Energy curves for Copper; 2020, https://www.skarnassociates.com/ghg/copper [retrieved 11/2022].

USGS. Commodity Statistics and Information; 2022, https://www.usgs.gov/centers/national-minerals-information-center/commodity-statistics-and-information [retrieved 07.11.22].

Wells M. Murrin Murrin nickel laterite deposit, WA. Canberra, Australia: CRC LEME; 2003.

The stripping ratio refers to 2010 and 2011 as described by Roberts and Francis (2014). The Woodie Woodie Mine stripping ratio varies widely depending on the pits currently worked and depth, and can range from 1:3.4 - 4.5:1 (arithmetic mean 2.4:1) Barker (2020).