Development of disaggregated energy use and greenhouse gas emission footprints in Canada’s iron, gold, and potash mining sectors

Anil Kumar Kattaa, Matthew Davisa, Amit Kumara,

a Department of Mechanical Engineering, 10-263 Donadeo Innovation Centre for Engineering, University of Alberta, Edmonton, Alberta T6G 1H9, Canada.

Supplementary Information

Table A1: Crude iron ore extracted and production of iron concentrate and pellets (million Mg)

| Year | NFL |  |  |  |  | QC |  |  | NU |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Crude ore | Concentrate production | Pellet production | DSO share | Metataconite ore share | Crude ore | Concentrate production | Pellet production | Crude ore | Concentrate production |
| 2010 | 56.6 | 21.5 | 15.8 | 0% | 100% | 44.7 | 15.8 | 9.5 | 0 | 0 |
| 2011 | 52.8 | 20.6 | 12.1 | 1% | 99% | 43.3 | 15.8 | 9.3 | 0 | 0 |
| 2012 | 62.6 | 23.4 | 12.8 | 3% | 97% | 46.9 | 15.7 | 9.0 | 0 | 0 |
| 2013 | 64.5 | 25.9 | 11.4 | 7% | 93% | 58.6 | 18.6 | 9.1 | 0 | 0 |
| 2014 | 53.8 | 21 | 8.7 | 0% | 100% | 66.8 | 24.0 | 10.0 | 0.3 | 0.3 |
| 2015 | 49.4 | 20 | 9.3 | 12% | 89% | 70.7 | 26.6 | 10.0 | 1.5 | 1.3 |
| 2016 | 51.1 | 19.8 | 9.8 | 8% | 92% | 68.6 | 25.7 | 9.9 | 3.3 | 3.2 |

Table A2: Activity variables of gold mining (million Mg)

| Province | Year | Ore and waste extraction | Ore milled | Open-pit ore mined | Underground ore mined | Ore processed in gold extraction | Ore processed in gold recovery |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Newfoundland & Labrador | 2010 | 999505 | 114517 | 128993 | 0 | 114517 | 114517 |
|  | 2011 | 1170989 | 184226 | 135669 | 97140 | 184226 | 184226 |
|  | 2012 | 1671312 | 378721 | 272854 | 92295 | 378721 | 378721 |
|  | 2013 | 2024371 | 373818 | 289743 | 85220 | 373818 | 373818 |
|  | 2014 | 2010194 | 395194 | 296152 | 90498 | 395194 | 395194 |
|  | 2015 | 2158550 | 417883 | 321532 | 74705 | 417883 | 417883 |
|  | 2016 | 2074366 | 401585 | 308992 | 71792 | 401586 | 401586 |
| Nunavut | 2010 | 14688000 | 2040000 | 2040000 | 0 | 3468000 | 2040000 |
|  | 2011 | 21439605 | 2977723 | 2977723 | 0 | 5062129 | 2977723 |
|  | 2012 | 34762000 | 3820000 | 3820000 | 0 | 6494000 | 3820000 |
|  | 2013 | 36456992 | 4142840 | 4142840 | 0 | 7042828 | 4142840 |
|  | 2014 | 36988400 | 4156000 | 4156000 | 0 | 7065200 | 4156000 |
|  | 2015 | 27423386 | 4032851 | 4032851 | 0 | 6855846 | 4032851 |
|  | 2016 | 32359596 | 4758764 | 4758764 | 0 | 8089899 | 4758764 |
| Saskatchewan | 2010 | 203958 | 203958 | 0 | 203958 | 203958 | 203958 |
|  | 2011 | 1105220 | 349086 | 403010 | 387862 | 440991 | 349086 |
|  | 2012 | 1179369 | 415376 | 447616 | 382612 | 555517 | 415376 |
|  | 2013 | 461258 | 428883 | 41506 | 387377 | 577766 | 428883 |
|  | 2014 | 350236 | 350236 | 29440 | 320796 | 420875 | 350236 |
|  | 2015 | 277368 | 277368 | 0 | 277368 | 277368 | 277368 |
|  | 2016 | 275981 | 275981 | 0 | 275981 | 275981 | 275981 |
| British Columbia | 2010 | 28237903 | 27351596 | 27351758 | 606817 | 7894596 | 0 |
|  | 2011 | 27367152 | 7730758 | 10756942 | 358156 | 7716856 | 0 |
|  | 2012 | 30452900 | 10148205 | 8121878 | 2026327 | 12121878 | 0 |
|  | 2013 | 31954066 | 12062221 | 7956738 | 4105483 | 16112738 | 0 |
|  | 2014 | 20798594 | 9428139 | 4548182 | 4879957 | 14191203 | 0 |
|  | 2015 | 11532233 | 6919735 | 1781799 | 5295936 | 12016735 | 0 |
|  | 2016 | 11347717 | 6809019 | 1753290 | 5211201 | 11824467 | 0 |
| Manitoba | 2010 | 0 | 275860 | 0 | 0 | 551720 | 275860 |
|  | 2011 | 486579 | 491150 | 0 | 486579 | 982300 | 491150 |
|  | 2012 | 615344 | 629276 | 0 | 615344 | 1258552 | 629276 |
|  | 2013 | 615344 | 629276 | 0 | 615344 | 1258552 | 629276 |
|  | 2014 | 629311 | 641710 | 0 | 629311 | 1283420 | 641710 |
| Yukon | 2010 | 262883 | 262883 | 262883 | 0 | 262883 | 262883 |
|  | 2011 | 234322 | 234322 | 234322 | 0 | 234322 | 234322 |
|  | 2012 | 264301 | 264301 | 264301 | 0 | 264301 | 264301 |
|  | 2013 | 298472 | 298472 | 298472 | 0 | 298472 | 298472 |
|  | 2014 | 296157 | 296157 | 296157 | 0 | 296157 | 296157 |
|  | 2015 | 298049 | 298049 | 298049 | 0 | 298049 | 298049 |
|  | 2016 | 522182 | 522182 | 522182 | 0 | 522182 | 522182 |
| Ontario | 2010 | 23960893 | 12021115 | 1084655 | 15629865 | 17559111 | 12021115 |
|  | 2011 | 25379411 | 12544963 | 884609 | 16423224 | 18446155 | 12544963 |
|  | 2012 | 31101337 | 14532035 | 2347235 | 17857302 | 20593494 | 14532035 |
|  | 2013 | 95668344 | 28780988 | 17918368 | 17547077 | 35015652 | 28780988 |
|  | 2014 | 98904506 | 34244604 | 18552723 | 18166526 | 39311952 | 32901521 |
|  | 2015 | 108773157 | 33691104 | 24231245 | 17309638 | 40082633 | 33691104 |
|  | 2016 | 109208249 | 33825868 | 24328170 | 17378876 | 40242963 | 33825868 |
| Quebec | 2010 | 4811279 | 7510084 | 0 | 4811279 | 11060384 | 7510084 |
|  | 2011 | 30802817 | 15433665 | 8502323 | 4445616 | 18750112 | 15433665 |
|  | 2012 | 47844793 | 18298240 | 14046526 | 4300562 | 18938546 | 18298240 |
|  | 2013 | 61062485 | 23037850 | 18081104 | 4799784 | 24681925 | 23037850 |
|  | 2014 | 66836330 | 25728778 | 19630945 | 7037867 | 28958462 | 25728778 |
|  | 2015 | 67776005 | 26217760 | 19965496 | 7160564 | 29589222 | 26217760 |
|  | 2016 | 68521541 | 26506155 | 20185116 | 7239330 | 29914703 | 26506155 |

Table A3: Gold production through various extraction and recovery technologies (kg)

| Province | Gold extraction/recovery technology |  | Year |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  | 2010 | 2011 | 2012 | 2013 | 2014 | 2015 |
| Newfoundland & Labrador | Gold extraction | Flotation and agitated cyanide leaching | 387 | 320 | 712 | 652 | 673 | 713 |
|  | Gold recovery | Merill Crowe | 387 | 171 | 383 | 476 | 466 | 506 |
|  |  | CIP, CIL | 0 | 149 | 329 | 176 | 206 | 207 |
|  | Post recovery | Electrowinning | 387 | 320 | 712 | 652 | 673 | 713 |
| Nunavut | Gold extraction | Gravity concentration | 2550 | 2600 | 3514 | 4134 | 4128 | 3665 |
|  |  | Agitated cyanide leaching | 5951 | 6066 | 8199 | 9646 | 9632 | 8552 |
|  | Gold recovery | Intensive cyanidation | 2550 | 2600 | 3514 | 4134 | 4128 | 3665 |
|  |  | CIP, CIL | 5951 | 6066 | 8199 | 9646 | 9632 | 8552 |
|  | Post recovery | Electrowinning | 8501 | 8666 | 11713 | 13780 | 13760 | 12218 |
| Saskatchewan | Gold extraction | Gravity concentration | 0 | 693 | 599 | 496 | 192 | 0 |
|  |  | Agitated cyanide leaching | 1513 | 1779 | 1886 | 1651 | 2111 | 2424 |
|  | Gold recovery | CIP, CIL | 1513 | 1779 | 1886 | 1651 | 2111 | 2424 |
|  | Post recovery | Direct smelting of gravity concentrate | 0 | 693 | 599 | 496 | 192 | 0 |
|  |  | Electrowinning | 1513 | 1779 | 1886 | 1651 | 2111 | 2424 |
| British Columbia | Gold extraction | Gravity concentration | 74 | 190 | 714 | 2091 | 7439 | 8719 |
|  |  | Agitated cyanide leaching | 148 | 233 | 0 | 0 | 0 | 0 |
|  |  | Flotation only | 4811 | 1399 | 2340 | 2910 | 2584 | 3177 |
|  |  | DMS and gravity concentration | 0 | 0 | 0 | 0 | 465 | 350 |
|  | Gold recovery | CIP, CIL | 148 | 233 | 0 | 0 | 0 | 0 |
|  | Post recovery | Electrowinning | 148 | 233 | 0 | 0 | 0 | 0 |
|  |  | Direct smelting of gravity concentrate | 74 | 190 | 125 | 60 | 82 | 111 |
|  |  | Smelting of concentrate | 4811 | 1399 | 2929 | 4941 | 10406 | 12135 |
| Manitoba | Gold extraction | Flotation and agitated cyanide leaching | 877 | 1497 | 1744 | 1744 | 1516 | 0 |
|  |  | Gravity concentration | 515 | 879 | 1024 | 1024 | 891 | 0 |
|  | Gold recovery | CIP, CIL | 877 | 1497 | 1744 | 1744 | 1516 | 0 |
|  | Post recovery | Electrowinning | 877 | 1497 | 1744 | 1744 | 1516 | 0 |
|  |  | Direct smelting of gravity concentrate | 515 | 879 | 1024 | 1024 | 891 | 0 |
| Yukon | Gold extraction | Gravity concentration | 31946 | 31199 | 27313 | 32121 | 35770 | 1520 |
| Ontario | Gold extraction | Flotation and agitated cyanide leaching | 9452 | 8360 | 8620 | 11202 | 10586 | 10181 |
|  |  | Gravity concentration | 16566 | 15349 | 13401 | 16411 | 17933 | 17359 |
|  |  | Agitated cyanide leaching | 28703 | 28843 | 2084 | 37815 | 43778 | 41956 |
|  |  | Cyanidation in grinding | 1761 | 2310 | 975 | 3067 | 3546 | 3374 |
|  |  | Flotation concentrate autoclave | 1350 | 1194 | 947 | 947 | 796 | 721 |
|  | Gold recovery | Merill Crowe | 705 | 542 | 710 | 868 | 1013 | 969 |
|  |  | Intensive cyanidation | 0 | 0 | 0 | 2527 | 4968 | 5500 |
|  |  | CIP, CIL | 38801 | 37855 | 38089 | 49095 | 54147 | 51889 |
|  |  | CIC | 1761 | 2310 | 2084 | 3067 | 3546 | 3374 |
|  | Post recovery | Electrowinning | 41267 | 40707 | 40884 | 55557 | 63674 | 61732 |
|  |  | Direct smelting of gravity concentrate | 16566 | 15349 | 13401 | 13883 | 12965 | 11858 |
| Quebec | Gold extraction | Flotation and agitated cyanide leaching | 7896 | 5747 | 5792 | 6750 | 8745 | 16889 |
|  |  | Gravity concentration | 31946 | 31199 | 6713 | 7079 | 9361 | 10541 |
|  |  | Agitated Cyanide leaching | 3066 | 8393 | 14263 | 20774 | 9257 | 12633 |
|  |  | Gravity concentration and oxidation | 2067 | 1884 | 1869 | 1773 | 1630 | 1601 |
|  | Gold recovery | Merill Crowe | 2528 | 1944 | 2508 | 1594 | 2212 | 1596 |
|  |  | Intensive cyanidation | 2258 | 2622 | 2520 | 1001 | 2169 | 3762 |
|  |  | CIP, CIL | 61140 | 17415 | 23029 | 28703 | 19472 | 31572 |
|  | Post recovery | Electrowinning | 65926 | 21981 | 28057 | 31298 | 23853 | 36931 |
|  |  | Direct smelting of gravity concentrate | 6384 | 5050 | 1673 | 5078 | 5140 | 4732 |

Table A4: Propane energy demand (GJ) in underground gold mining

| Province | Average ambient air temperature (0C) | Propane energy consumption (GJ) |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | 2010 | 2011 | 2012 | 2013 | 2014 | 2015 |
| Newfoundland and Labrador | -10 | 0.00 | 0.01 | 0.01 | 0.00 | 0.00 | 0.00 |
| Saskatchewan | -15 | 0.01 | 0.03 | 0.03 | 0.03 | 0.02 | 0.02 |
| British Columbia | -5 | 0.02 | 0.01 | 0.01 | 0.03 | 0.04 | 0.04 |
| Manitoba | -18 | 0.00 | 0.04 | 0.05 | 0.05 | 0.05 | 0.00 |
| Yukon | -21 | 0.00 | 0.03 | 0.05 | 0.05 | 0.00 | 0.00 |
| Quebec | -12 | 0.27 | 0.25 | 0.24 | 0.27 | 0.39 | 0.40 |
| Ontario | -12 | 0.88 | 0.92 | 1.00 | 0.98 | 1.02 | 0.97 |

Table A5: Potash production through different mining methods

| Extraction method | Province | 2010 | 2011 | 2012 | 2013 | 2014 | 2015 | 2016 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Conventional (million Mg) | Saskatchewan | 12.2 | 14.2 | 13.2 | 13.6 | 13.5 | 15.8 | 16.3 |
|  | New Brunswick | 0.6 | 0.7 | 0.7 | 0.6 | 0.6 | 0.7 | 0.7 |
| Solution (million Mg) | Saskatchewan | 1.9 | 2.6 | 2.6 | 2.5 | 2.2 | 2.4 | 2.4 |
| Total (million Mg) | Saskatchewan | 14.0 | 16.7 | 15.8 | 16.1 | 15.7 | 18.2 | 18.8 |
|  | New Brunswick | 0.6 | 0.7 | 0.7 | 0.6 | 0.6 | 0.7 | 0.7 |
| Conventional (%) | Saskatchewan | 86.7 | 84.5 | 83.6 | 84.6 | 86.0 | 86.8 | 86.7 |
|  | New Brunswick | 100.0 | 100.0 | 100.0 | 100.0 | 100.0 | 100.0 | 100.0 |
| Solution (%) | Saskatchewan | 13.3 | 15.5 | 16.4 | 15.4 | 14.0 | 13.2 | 13.3 |

Table A6: Electricity grid emission intensity factor (grams CO2 eq./kilowatt-hour)

| Province | 2016 |
| --- | --- |
| British Columbia (BC) | 13 |
| Saskatchewan (SK) | 543 |
| Manitoba (MB) | 39 |
| Ontario (ON) | 5 |
| Quebec (QC) | 6 |
| New Brunswick (NB) | 215 |
| Newfoundland and Labrador (NFL) | 14 |
| Yukon (YK) | 0 |
| Nunavut (NU) | 639 |

Table A7: Emission factors used in the model (Heaps, 2016)

| Fuel type | Emission factor |  |  |
| --- | --- | --- | --- |
|  | CO2 (kg/TJ) | CH4 (kg/TJ) | N2O (kg/TJ) |
| Natural gas | 56100 | 1 | 0.1 |
| Diesel | 74100 | 3.9 | 3.9 |
| Heavy fuel oil | 77400 | 3 | 0.6 |
| Coke | 94600 | 1 | 1.5 |

# Energy use in iron ore extraction and haulage

The extraction stage involves the removal of overburden to reveal the underlying ore body. The ore body is subjected to drilling and blasting operations and is then loaded by electrical shovels, rope shovels, and hydraulic excavators onto haul trucks (Härkisaari, 2015). Drilling is done with ammonium nitrate fuel oil (ANFO) loader trucks, diamond drills, rotary drills, percussion drills, and drill boom jumbos, which run on electricity, diesel or compressed air (US Department of Energy, 2007). Soft ores are dug rather than drilled. Digging is a process of excavating or making a passage in the ore body for blasting (US Department of Energy, 2007). The current study is limited to the use of fuels for energy consumption alone and hence the blasting operation, which uses emulsions, is excluded from the analysis. Haulage is required to transport the ore to the processing facility. The haulage units include diesel powered off-road dump trucks, conveyors, and trains.

# Iron ore processing energy use

Processing involves upgrading and recovering the metal through beneficiation, which involves comminution and concentration to remove impurities and improve ore quality (Härkisaari, 2015). Comminution is the crushing and grinding of the ore to liberate minerals from the ore matrix and increase the surface area for higher reactivity. The comminution circuit can have a few to several stages of crushing, grinding, and screening (Jankovic, 2015). Gyratory, jaw, and cone crushers compress and break large rocks into coarse particles. After crushing, autogenous/semi-autogenous (AG/SAG) mills, ball mills, or pebble mills are used to grind the ore into even smaller uniformed-sized particles. Ball mills have a higher energy intensity than either crushing or the AG/SAG mill as they produce high grade concentrates suitable for pelletizing.

The concentration processes are gravity separation (to separate gangue and waste), magnetic separation (to separate magnetite), and flotation (to separate hematite) (US Department of Energy, 2002b). Electricity is the primary source of fuel in these processes. Gravity separation techniques include dense medium separation (DMS), jigging, and spiraling (Maré et al., 2015). The DMS process is the best choice for a non-porous feed. The separation medium is a dense liquid made up of very fine ferrosilicon particles in water. In the jigging process, a bed of ore is formed on a screen deck inside a water-filled chamber. A pulsing cycle, created with upward and downward movements of the water column, allows heavier particles to settle faster than lighter particles. Spiraling involves a combination of centrifugal and fluid-related responses to separate fines and coarse particles, especially for wet fines processing. Hydroclone classifiers are used to separate particles by shape, size, and specific gravity in grinding circuits. Magnetic separation is used to remove non-magnetic materials from the ore. The flotation process, unlike the others, is energy intensive and expensive. In general, it is used after the ore has been enriched by other separation techniques. In the flotation process, the ore surface is treated with chemicals and suspended in a mechanically agitated and aerated water chamber. The valuable hydrophobic portion of the ore attaches to the air bubbles and rises to the surface for collection. Jankovic (2015) discusses the processing methods in detail. The separation and concentration process energy intensities were obtained from NRCan (Natural Resources Canada, 2005a) and literature (Griffing and Overcash, 2010).

# Pelletization energy use

In the pretreatment process, the ore is ground into fines, dried, and pre-wetted for balling (Yamaguchi et al., 2010). The balling equipment consumes electricity and uses centrifugal force to form spheroids that are dried, fired, and then cooled in an indurating furnace. Hot and cold gases are moved in the furnace by fans or blowers. The energy intensities of the pelletizing operations were estimated from literature (Griffing and Overcash, 2010; Singh et al., 2015). The shares of coke and heavy fuel oil in the firing process were estimated by taking the ratio of energy demand for the these fuels from NRCan’s Energy Use Database (Natural Resources Canada, 2018).

# Gold ore extraction and comminution energy use

Ore is extracted through open-pit and underground mining (Mining Association of Canada, 2016). Apart from drilling and blasting operations, underground mining requires underground crushing, ore hoisting, ventilation, and backfilling (Natural Resources Canada, 2005b). The energy intensities for ore extraction processes were obtained from previously developed benchmarks (Natural Resources Canada, 2005b). The energy intensity is defined as MJ/Mg of O+W removed for open-pit ore extraction processes, MJ/Mg of O for underground ore extraction, and MJ/Mg of ore processed for comminution processes, and is shown in Table 2b. Ore haulage using diesel equipment has the highest energy intensity in open pit mines. For underground mines, ventilation is responsible for about 50% of the total ore extraction energy demand.

# Gold extraction energy use

Flotation, gravity concentration, and leaching (heap leaching or tank leaching) are used to extract gold from ore (Marsden, 2006). Leaching is done by applying lime, sodium, or potassium cyanide solution to open heaps or to ore slurry in tanks; the former is used to extract gold from low-grade ores and the latter for high-grade ores (Marsden, 2006; US Department of Energy, 2002a). Gravity concentration is used to separate free elemental gold in the ore before the leaching process. Flotation is used prior to leaching if the ore contains sulphides (Norgate and Haque, 2012). The slurry, flotation, and gravity concentrate undergo processes to recover gold. The energy intensity is defined as MJ/Mg of ore processed. Electricity and natural gas are the fuels used in these processes; their energy intensities are shown in Table 2b.

# Gold recovery energy use

In the CIP process, the activated carbon granules are added to a series of agitated slurry tanks to adsorb the gold. As the slurry flows from tank to tank, the gold in the slurry gets loaded onto the carbon. The CIL process is used to treat carbonaceous ores when leaching and adsorption occur in a single process. The CIC operation is primarily used for heap leach solutions in which the solution flows upward through a series of fluidized bed columns (Kubach, 1994). The energy demand in these processes is from the use of electricity to agitate and pump the slurry. The energy intensities for the end-use processes in the recovery stage are shown in Table 2b.

# Post-recovery energy use

The energy intensity in terms of MJ/Mg of product (Au) is shown in Table 2b.

# Propane energy use calculation inputs

The ratio of mass air flow required per mass ore produced is 2.4 for the block caving mining method and 11.8 for non-block cave mining methods (Wallace, 2001). The methods used by mining companies in Canada were obtained from SEDAR (SEDAR, 2017). The recommended air temperature is 50° C, the efficiency of the propane heater is 90%, the number of months mine air heating is required was considered to be 3, and the specific heat of air is 1.005 kJ/kg.K (Mine Wiki, 2018). The average ambient air temperatures were obtained from Environment Canada’s Temperature Climatology Map (Government of Canada, 2018).

# References

Government of Canada, 2018. Climatology of temperature and precipitation. https://weather.gc.ca/saisons/image_e.html?format=clim_stn&season=jfm&type=temp (accessed April 2018).

Griffing, E., Overcash, M., 2010. Iron ore mining and pelletizing in US-Chemical Life Cycle Database (1999-Present). www.environmentalclarity.com (accessed September 2017).

Härkisaari, P., 2015. Wear and friction effects on energy consumption in the mining industry, MSc thesis. Tampere University of Technology, Tampere, Finland.

Heaps, C.G., 2016. Long-range Energy Alternatives Planning (LEAP) system. [Software version 2018.0.1.2] Stockholm Environment Institute Somerville, MA, USA. https://www.energycommunity.org (accessed January 2017).

Jankovic, A., 2015. Developments in iron ore comminution and classification technologies, Iron Ore. Elsevier, pp. 251-282.

Kubach, C., 1994. Gold mining and processing in South Africa. http://www.mine-engineer.com/mining/mineral/gold.htm (accessed November 2017).

Maré, E., Beven, B., Crisafio, C., 2015. Developments in nonmagnetic physical separation technologies for hematitic/goethitic iron ore, Iron Ore. Elsevier, pp. 309-338.

Marsden, J., 2006. Overview of gold processing techniques around the world. Minerals and Metallurgical Processing 23(3), 121-125.

Mine Wiki, 2018. Mine Design - Ventilation air heating. http://minewiki.engineering.queensu.ca/mediawiki/index.php/Ventilation_air_heating (accessed April 2018).

Mining Association of Canada, 2016. Facts and Figures of the Canadian Mining Industry. http://mining.ca/resources/reports (accessed March 2017).

Natural Resources Canada, 2005a. Benchmarking the Energy Consumption of Canadian Open-pit Mines. http://www.publications.gc.ca/site/eng/287279/publication.html (accessed August 2017).

Natural Resources Canada, 2005b. Benchmarking the Energy Consumption of Canadian Underground Bulk Mines. http://publications.gc.ca/site/eng/287264/publication.html (accessed October 2017).

Natural Resources Canada, 2018. Comprehensive Energy Use Database. http://oee.nrcan.gc.ca/corporate/statistics/neud/dpa/menus/trends/comprehensive_tables/list.cfm (accessed April 2018).

Norgate, T., Haque, N., 2012. Using life cycle assessment to evaluate some environmental impacts of gold production. Journal of Cleaner Production 29, 53-63.

SEDAR, 2017. System for Electronic Document Analysis and Retrieval. https://www.sedar.com/homepage_en.htm (accessed August 2017).

Singh, G., Choudhary, R., Vardhan, H., Aruna, M., Akolkar, A., 2015. Iron ore pelletization technology and its environmental impact assessment in eastern region of India–a case study. Procedia Earth and Planetary Science 11, 582-597.

US Department of Energy, 2002a. Energy and Environmental Profile of the US Mining Industry - Gold and Silver. https://www.energy.gov/sites/prod/files/2013/11/f4/gold-silver.pdf (accessed October 2017).

US Department of Energy, 2002b. Energy and Environmental Profile of the US Mining Industry - Iron. https://www.energy.gov/sites/prod/files/2013/11/f4/iron.pdf (accessed October 2017).

US Department of Energy, 2007. Mining Industry Energy Bandwidth Study. https://www.energy.gov/sites/prod/files/2013/11/f4/mining_bandwidth.pdf (accessed April 2018).

Wallace, K., 2001. General operational characteristics and industry practices of mine ventilation systems. Proceedings of the 7th International Mine Ventilation Congress (Ed: S. Wasilewski).

Yamaguchi, S., Fujii, T., Yamamoto, N., Nomura, T., 2010. Kobelco pelletizing process. Kobelco Technology Review 29, 58-59.

Corresponding author: Tel.: +1-780-492-7797

E-mail: Amit.Kumar@ualberta.ca (Amit Kumar).